# Supplementary Material

Photocatalytic Degradation of PFAS Under Surface Water Matrix Conditions Using an Adsorptive Photocatalyst

Yangmo Zhu1,2, Rodney Nelson Leary III3, Tianyuan Xu4, Ke He5, Lee Blaney5, Xiaodi Hao1, Dongye Zhao2,3,*

1 State Key Laboratory of Urban Stormwater System and Water Environment, Ministry of Education/Sino-Dutch R&D Centre for Future Wastewater Treatment Technologies, Beijing University of Civil Engineering & Architecture, Beijing, 100044, PR China

2 Department of Civil & Environmental Engineering, Auburn University, Auburn, AL 36849, USA

3 Department of Civil, Construction & Environmental Engineering, San Diego State University, San Diego, CA 92182, USA

4 School of Resource and Geosciences, China University of Mining and Technology, Xuzhou, Jiangsu, 221116, PR China

5 Department of Chemical, Biochemical, and Environmental Engineering, University of Maryland Baltimore County, MD 21250, USA

Contents:

Text sections: 7

Tables: 5

Figures: 8

* Corresponding author. Email: dzhao2@sdsu.edu (D. Zhao)

# S1. Chemicals and materials

Nano-TiO2 (Degussa P25, 80 wt.% anatase and 20 wt.% rutile) was purchased from Evonik (Worms, Germany). Filtrasorb-400® (F400) granular activated carbon (GAC) was obtained from Calgon Carbon Corporation (Moon Township, PA, USA). PFOS, sodium nitrate, sodium sulfate, sodium calcium chloride, sodium chloride, potassium chloride, magnesium chloride, iron(III) chloride hexahydrate, anhydrous gallium chloride, methanol, and sodium hydroxide were acquired from VWR International (Radnor, PA, USA). The 28 analytical PFAS standards and 23 mass-labeled PFAS (MPFAS), which were used as extracted or non-extracted internal standards, were purchased from Wellington Laboratories Inc. (Guelph, Ontario, Canada). Table S2 shows the names, acronyms, and CAS numbers for the 28 PFAS analytes, and Tables S2 and S3 summarize the liquid chromatography with triple quadrupole tandem mass spectrometry (LC-MS/MS) operational parameters for the PFAS and MPFAS, respectively. All chemicals were of the analytical-grade or higher, and all solutions were prepared using deionized water (18.2 MΩ-cm).

# S2. Preparation of Ga/TNTs@AC

Ga/TNTs@AC was prepared via a modified, one-step, hydrothermal treatment approach (Liu et al., 2016; Zhu et al., 2021). Typically, 1.2 g F400 GAC and 1.2 g TiO2 were added to 66.7 mL of 10 M NaOH. The sealed mixture was stirred for 12 h, and then transferred to a 100-mL Teflon reactor enclosed in a stainless-steel cup. The reactor was heated to 130 °C, maintained for 72 h, and then cooled to room temperature. After 1 h of gravity settling, two distinct layers were observed. The upper layer was removed, and the lower layer, which contained TNTs@AC, was washed with deionized water until neutral pH. The material was dried at 105 °C for 8 h. Subsequently, 1 g dried TNTs@AC was dispersed in 80 mL deionized water, and then 4 mL of a GaCl3 solution (5 g/L as Ga) was added dropwise to the suspension. The mass ratio of Ga-to-TNTs@AC was fixed at 2 wt.% based on our prior work (Zhu et al., 2021). The mixture was equilibrated for 3 h, after which >99% of Ga was incorporated to TNTs@AC. After 1 h of gravity settling, the solids were dried at 105 °C for 8 h, and the resulting particles were calcined at 550 °C for 3.5 h in a nitrogen atmosphere (2.5 L/min) with a temperature ramp of 10 °C/min. The resulting composite was denoted as Ga/TNTs@AC. No organofluorine or inorganic fluoride were detected in the material.

# S3. Adsorption kinetics and isotherms

FSW spiked with 100 µg/L PFOS was employed in preliminary batch adsorption kinetics and isotherm experiments. PFOS was selected as the probe compound because it was the most dominant PFAS present in the surface water. Adsorption kinetics were assessed in 45-mL HDPE vials by adding 40 mg Ga/TNTs@AC to 40 mL FSW spiked with 100 µg/L PFOS. The vials were kept in the dark at 25 °C and rotated at 70 rpm. Duplicate vials were sacrificially sampled at predetermined times. The equilibrium pH was 7.0 ± 0.1. After passing the samples through a 0.22-µm polyethersulfone (PES) membrane, filtrates were analyzed for aqueous-phase PFOS concentrations. Control studies confirmed that >99% PFOS was recovered in the filtrates.

Similar experimental protocols were applied to generate adsorption isotherms. Batch reactors were rotated for 24 h, which was sufficient to reach equilibrium. The Ga/TNTs@AC dose was maintained at 1 g/L, but the initial PFOS concentration in FSW was varied (i.e., 0.1, 0.5, 1, 5, 10, 15, 20 mg/L) to reach different endpoints on the isotherm. PFOS uptake was calculated by mass balance using the initial and final concentrations. For comparison, isotherms were also constructed for PFOS in ultrapure water to evaluate matrix effects imposed by the surface water.

# S4. Photocatalysis kinetics

Batch photocatalysis experiments were carried out in a Rayonet RPR-100 UV-reactor (Southern New England Ultraviolet Co., Branford, CT, USA) equipped with 16 RPR-2537 Å lamps. The system was maintained at approximately 35 °C. Following adsorption equilibrium, 0.12 g PFAS-laden Ga/TNTs@AC was separated by gravity settling for 1 h. Subsequently, 99% of the supernatant was removed, and the solids were transferred into a quartz dish (6×1.5 cm, outer diameter × height) with a quartz cover. Deionized water (10 mL) was added to the dish, which was then placed in the center of the photoreactor. The light intensity was 128 and 210 W/m2 at the center (6.81 cm from all lamps) and edge (3.81 cm from the nearest lamp), respectively, of the quartz dish. During irradiation, the Ga/TNTs@AC mixture was stirred every 15 min. At specific sampling times (i.e., 1, 2, 3, 4 h), the dishes were removed from the reactor and allowed to settle for 15 min by gravity. The supernatant was sacrificially filtered through 0.22-µm PES membranes, and the filtrate was analyzed for PFAS and fluoride. To measure the residual solid-phase PFOS concentration, spent Ga/TNTs@AC was subjected to an 8-h extraction with 40 mL methanol at 80 °C in tightly sealed vials (Li et al., 2020). Control tests with pre-irradiated Ga/TNTs@AC confirmed the PFOS recovery was >95% and the absence of fluoride in 20 mL of 1 M NaOH extractant. In addition, the recovery for other target PFAS (PFHxS, PFNS, PFPeS, and PFBS) exceeded >96%. All tests were carried out in duplicate.

# S5. Fixed-bed column breakthrough tests

Compared to adsorption in batch systems, fixed-bed column reactors allow for more efficient adsorption, because PFAS are concentrated on the Ga/TNTs@AC media in a manner that reaches equilibrium with the influent concentration. For this reason, fixed-bed column experiments were conducted and run to determine the breakthrough profile for PFOS. The experimental setup included an HPLC pump, a glass column (10×100 mm, inner diameter × length) with two fixed end pieces, and a fraction collector. The column was packed with 1.97 g Ga/TNTs@AC, which yielded a bulk bed volume of 4.32 cm3. The column adsorption test was initiated by pumping surface water spiked with 100 µg/L PFOS through the column in downflow mode. Air bubbles were removed by tapping the column with a rubber tube to ensure even packing of the material. The flowrate was maintained at 0.54 mL/min, resulting in an empty bed contact time (EBCT) of 8.0 min and a superficial liquid velocity (SLV) of 1.1×10-4 m/s. The breakthrough curve was recorded by monitoring PFOS concentrations in the effluent over time. After saturation, the Ga/TNTs@AC media were removed from the column and oven dried at 105 °C for 8 h. The mass of recovered particles was 1.90 g (i.e., 3.6% mass loss). The dried particles were thoroughly mixed and split into two portions. One portion was used to confirm the mass of PFAS adsorbed to Ga/TNTs@AC during the column test, and the other was subjected to the UV irradiation for photocatalytic degradation of the sorbed PFAS (see Section 2.6.2).

PFAS bound to the Ga/TNTs@AC media were extracted into methanol (i.e., 0.12 g solid in 40 mL methanol) at 80 °C for 8 h. After centrifugation at 2500 rpm for 10 min, the supernatant was transferred to a clean vial, and then a second extraction was conducted under the same conditions to ensure maximum PFAS recovery. PFAS concentrations were measured in the extracts.

# S6. PFAS analysis by LC-MS/MS

The original and filtered surface water, experimental samples, and extracts from the adsorbent photocatalysts were shipped to the University of Maryland Baltimore County for PFAS analysis in accordance with EPA Method 1633 (EPA, 2024). Aqueous samples were fortified with 5 ng mass-labeled PFAS (MPFAS) extracted internal standards (EIS) (Table S2), vortexed, and passed through a solid-phase extraction (SPE) cartridge containing a mixed-mode, weak-anion exchange (WAX) sorbent to capture PFAS and MPFAS. The WAX cartridge was conditioned with 3 mL of 0.1% ammonium hydroxide in methanol followed by 3 mL of 10 mM ammonium acetate solution (pH 7.0). Samples were loaded at 1-3 mL/min by adjusting the vacuum. Before loading, 3 mL of deionized water was added to the sample container to minimize residue loss. After loading, 3 mL of 1 mM hydrochloric acid solution (pH 3.0) was applied for washing, followed by 2 mL of 50% methanol for the same purpose. Then, 3 mL of acetonitrile with 5% ammonium hydroxide was used to rinse the sample container (i.e., “bottle rinsate”); then, this solution was used to elute analytes from the SPE cartridge by gravity. The final extract was evaporated to dryness under nitrogen, reconstituted with 0.25 mL of methanol containing 10 g/L of non-extracted internal standards (NIS), vortexed to ensure uniform conditions, adjusted to 0.5 mL with 10 mM ammonium acetate, and vortexed again. The reconstituted samples were transferred into 750-µL polypropylene LC vials and stored at 4 °C before analysis within 48 h. If the measured concentration of a target analyte was above the calibration range, additional dilution was conducted with proper spiking of NIS.

The 28 PFAS and 23 MPFAS were measured with one LC-MS/MS method using an UltiMate 3000 LC coupled to a Thermo TSQ Quantum Access Max triple quadrupole tandem mass spectrometer (LC-MS/MS; Thermo Fisher Scientific; Waltham, MA, USA). Samples (50 µL) were injected onto a Waters XBridge BEH C18 (2.1×5 mm, 2.5 µm) guard column connected in series to a Waters XBridge BEH C18 (2.1×150 mm, 2.5 µm) analytical column. Analytes were separated using a 15-min gradient elution method with (A) methanol with 10 mM ammonium acetate and (B) water with 10 mM ammonium acetate (pH 7.0). The elution scheme was as follows: 45% A for 2 min; ramp to 90% A over 5 min; constant at 90% A for 3 min; ramp to 45% A within 1 min; and, constant at 45% A for 4 min. The column temperature was 40 °C, and the eluent flow rate was 200 µL/min. Negative electrospray ionization was employed for all analytes. At least one product ion was selected for quantitation, and one product ion was employed for confirmation; PFBA, PFPeA, MPFBA, and M5PFPeA were exceptions in accordance with EPA Method 1633 (EPA, 2024). The molecular weight, retention time, specific ion transitions, and ion transition ratios are presented in Table S3 for the 28 PFAS and Table S4 for the 23 MPFAS. The scan time was set to 0.05 s (i.e., 20 scan events per second), and the scanning window was set to 4 min with the retention time as the midpoint. In this 15-min method, at least 15 scans were acquired across the chromatographic peak for each analyte.

The instrumental limits of detection (LODs) and quantitation (LOQs) were determined based on the responses of (i) PFAS standard solutions prepared in deionized water and (ii) instrumental blanks (i.e., deionized water with NIS) for multiple injections (n = 6). The LODs and LOQs were calculated for signal-to-noise ratios of 3 and 10, respectively. Instrumental blanks were also used to confirm the absence of PFAS contamination in the LC-MS/MS system prior to sample analysis. The method detection limits (MDLs) and method quantitation limits (MQLs) were estimated using the LODs and LOQs, SPE concentration factors, and analyte recovery; note, 100% recovery was assumed for MDL and MQL calculations, but actual recovery was used for real samples. The LOQs and MQLs are summarized in Table S3; note that LODs and MDLs can be calculated by dividing the LOQs and MQLs by 3.3, respectively. Eleven calibration standards were generated at 0.10, 0.25, 0.50, 0.75, 1.0, 2.5, 5.0, 7.5, 10, 15, and 25 µg/L. The calibration curves and linearity (as coefficient of determination, R2) are summarized in Figure S2 and Table S3. The R2 values were greater than 0.99 for all PFAS. The first validated calibration standard was identified as the lowest concentration within 70-130% of the true value and a signal-to-noise ratio greater than 10; specific values are reported in Table S3 for each PFAS.

Typical recoveries of the 28 PFAS spiked in deionized water (i.e., laboratory control samples) and surface water are presented in Figure S3. In general, PFAS recovery efficiencies from the surface water samples were similar to PFAS recoveries from deionized water. The mean recovery ranged from 49% to 107%, and most recoveries of individual PFAS were similar to those reported in EPA Method 1633 (EPA, 2024). The slightly lower recoveries of PFOSA were attributed to losses during the washing step; however, the solvent washing step significantly reduced matrix effects for other PFAS. Results from the overall SPE protocol were highly reproducible, and the highest standard deviation was 17% for PFOS and PFDoA. The relative percent difference between the matrix spike and matrix spike duplicate was less than 30% for all 28 PFAS.

# S7. PFOS analysis by LC-Orbitrap-MS

The concentrations of PFOS and its photocatalytic transformation products in ultrapure experimental water samples were determined using a Vanquish Flex Binary UHPLC system (Thermo Fisher Scientific) coupled to an orbitrap mass spectrometer (Orbitrap Exploris TM120, Thermo Fisher Scientific) with negative-mode electrospray ionization. A delay column (HypersilGOLD, 1.9 µm, 175 Å, 3×50 mm) was placed between the pump and autosampler to remove background species. 13C8 mass-labeled PFOS (20 µg/L) was used as the internal standard. Samples (10 μL) were injected onto a C18 column (Luna C18(2), 3 µm, 100 Å, 2×50 mm with a 2×4 mm guard cartridge (Phenomenex). Gradient elution was performed using a mobile phase consisting of (A) 2 mM ammonium acetate (pH 4.7) and (B) 100% acetonitrile. The flow rate of the mobile phase was set to 0.2 mL/min. The gradient conditions were as follows: 70% A for 0.3 min; ramp to 5% A for 3.4 min; hold for 0.7 min; ramp to 70% A for 1.2 min; and re-equilibrate for 1.4 min. The total run time was 7 min. The capillary, sample cone, and extraction cone voltages were set to 2.8 kV, 30 V, and 4.0 V, respectively. The source temperature was 100 °C, and the desolvation temperature was maintained at 300 °C with a gas flow rate of 600 L/h. The TOF/MS scan was 1 s for the m/z range of 150 – 600 with a 0.02 s inter-scan delay using the centroid data format. A 0.2 mg/L solution of Leucine encephalin was used as the lock mass reference standard for instrument tuning and calibration.

At least five PFOS standards with concentrations ranging from 1 to 90 µg/L were used to develop calibration curves before analysis of experimental samples. The relative standard deviation for all analytes were within ±20%, and the R2 values were  0.99 to meet the initial calibration criteria. A secondary source standard was used to validate the initial calibration, and analyte concentrations were within ±30% of their true value. After every 10 samples or at the end of the sequence, two consecutive calibration verification standards were analyzed for quality assurance and quality control purposes. The concentrations were within ±30% of their true values from the LOQ (5 µg/L) to the mid-level calibration concentration.

# Tables

# Table S1. Summary of recent studies related to PFAS photodegradation.

| Material | Target contaminant | Light source | Experimental conditions | Degradation efficiency (%) | Reference |
| --- | --- | --- | --- | --- | --- |
| PTI/Bi/Bi5O7I | PFOA | 300 Xe lamp | C0=30 ppm | 94.8 | (Huang et al., 2024) |
|  |  |  | Time=3 h |  |  |
|  |  |  | pH=3 |  |  |
|  |  |  | 298 K |  |  |
| UV/Fe3+ | PFOA | 254 nm UV | CPFOA0=24 µM | 73.6 | (Liu et al., 2022) |
|  |  |  | CFe3+=25µM |  |  |
|  |  |  | Time = 4 h |  |  |
|  |  |  | pH = 4.2 |  |  |
|  |  |  | 298 K |  |  |
| Fe/TNTs@AC | PFOA | 254 nm (210 W/m2) | CPFOA0=100 µg/L | >90.0 | (Li et al., 2020) |
|  |  |  | Time= 4 h |  |  |
|  |  |  | pH = 7.0 ± 0.3 |  |  |
|  |  |  | 25 °C |  |  |
|  |  |  | Material dosage = 1 g/L |  |  |
|  |  |  | Fe content = 1 wt.% |  |  |
|  |  |  | Solution volume = 40 mL |  |  |
| Ga/TNTs@AC | PFOS | 254 nm (210 W/m2) | CPFOs0=100 µg/L | 75.0 | (Zhu et al., 2021) |
|  |  |  | Time= 4 h |  |  |
|  |  |  | pH = 7.0 ± 0.1 |  |  |
|  |  |  | Material dosage = 3 g/L |  |  |
|  |  |  | Ga content = 2 wt.% |  |  |
| Bi/TNTs@AC | GenX | 254 nm (210 W/m2) | CGenX0=100 µg/L | 70.0 | (Zhu et al., 2022) |
|  |  |  | Time= 4 h |  |  |
|  |  |  | pH = 7.0 ± 0.1 |  |  |
|  |  |  | Material dosage = 1 g/L |  |  |
|  |  |  | Bi content = 3 wt.% |  |  |
| BEA-topology zeolite | PFOA | 350 W Xe lamp | CPFOA0=50 µg/L | 94.1 | (Li et al., 2025) |
|  |  |  | Material dosage = 0.5 g/L |  |  |
|  |  |  | Time= 48 h |  |  |
|  |  |  | pH = 7.0 ± 0.1 |  |  |

# Table S2. Names, acronyms, and CAS numbers for PFAS measured in the surface water samples.

| Name | Acronym | CAS number |
| --- | --- | --- |
| Perfluorobutanoic acid | PFBA | 375-22-4 |
| Perfluoropentanoic acid | PFPeA | 2706-90-3 |
| Perfluorohexanoic acid | PFHxA | 307-24-4 |
| Perfluoroheptanoic acid | PFHpA | 375-85-9 |
| Perfluorooctanoic acid | PFOA | 335-67-1 |
| Perfluorononanoic acid | PFNA | 375-95-1 |
| Perfluorodecanoic acid | PFDA | 335-76-2 |
| Perfluoroundecanoic acid | PFUnA | 2058-94-8 |
| Perfluorododecanoic acid | PFDoA | 307-55-1 |
| Perfluorotridecanoic acid | PFTriA | 72629-94-8 |
| Perfluorotetradecanoic acid | PFTreA | 376-06-7 |
| Perfluorobutane sulfonic acid | PFBS | 375-73-5 |
| Perfluoropentane sulfonic acid | PFPeS | 2706-91-4 |
| Perfluorohexane sulfonic acid | PFHxS | 355-46-4 |
| Perfluoroheptane sulfonic acid | PFHpS | 375-92-8 |
| Perfluorooctane sulfonic acid | PFOS | 1763-23-1 |
| Perfluorononane sulfonic acid | PFNS | 68259-12-1 |
| Perfluorodecane sulfonic acid | PFDS | 335-77-3 |
| 4:2 fluorotelomer sulfonic acid | 4:2 FtS | 757124-72-4 |
| 6:2 fluorotelomer sulfonic acid | 6:2 FtS | 27619-97-2 |
| 8:2 fluorotelomer sulfonic acid | 8:2 FtS | 39108-34-4 |
| Perfluorooctanesulfonamide | PFOSA | 754-91-6 |
| 2-(N-ethylperfluorooctanesulfonamido) acetic acid | N-EtFOSAA | 2991-50-6 |
| 2-(N-methylperfluorooctanesulfonamido) acetic acid | N-MeFOSAA | 2355-31-9 |
| Hexafluoropropylene oxide dimer acid | HFPO-DA | 13252-13-6 |
| 4-dioxa-3H-perfluorononanoate | ADONA | 919005-14-4 |
| 9-chlorohexadecafluoro-3-oxanonane-1-sulfonate | 9Cl-PF3ONS | 73606-19-6 |
| 11-chloroeicosafluoro-3-oxaundecane-1-sulfonate | 11Cl-PF3OUdS | 763051-92-9 |

# Table S3. LC-MS/MS operational parameters and select method performance metrics for the 28 PFAS analytes.

| Compound | MW a | Ion transitions b | Ratio c | RT d | 1st cal. e | LOQ f | MQL g | R2 | Internal standard h |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PFBA | 214 | 212.9 → 168.9 | - | 3.61 | 0.1 | 0.1 | 2 | 0.992 | MPFBA |
|  |  | - |  |  |  |  |  |  |  |
| PFPeA | 264 | 262.9 → 218.9 | - | 6.41 | 0.1 | 0.1 | 2 | 0.993 | M5PFPeA |
|  |  | - |  |  |  |  |  |  |  |
| PFHxA | 314 | 312.9 → 268.9 | 0.01 | 9.01 | 0.1 | 0.25 | 5 | 0.997 | MPFHxA |
|  |  | 312.9 → 118.9 |  |  |  |  |  |  |  |
| PFHpA | 364 | 362.9 → 318.9 | 0.15 | 9.71 | 0.1 | 0.25 | 5 | 0.995 | M4PFHpA |
|  |  | 362.9 → 168.9 |  |  |  |  |  |  |  |
| PFOA | 414 | 412.9 → 368.9 | 0.20 | 10.15 | 0.5 | 0.5 | 10 | 0.991 | MPFOA |
|  |  | 412.9 → 168.9 |  |  |  |  |  |  |  |
| PFNA | 464 | 462.9 → 418.9 | 0.20 | 10.52 | 0.1 | 0.25 | 5 | 0.997 | MPFNA |
|  |  | 462.9 → 168.9 |  |  |  |  |  |  |  |
| PFDA | 514 | 512.9 → 468.9 | 0.10 | 10.90 | 0.1 | 0.25 | 5 | 0.993 | MPFDA |
|  |  | 512.9 → 218.9 |  |  |  |  |  |  |  |
| PFUnA | 564 | 562.9 → 518.9 | 0.05 | 11.28 | 0.5 | 0.5 | 10 | 0.993 | MPFUdA |
|  |  | 562.9 → 168.9 |  |  |  |  |  |  |  |
| PFDoA | 614 | 612.9 → 568.9 | 0.05 | 11.67 | 0.1 | 0.25 | 5 | 0.998 | MPFDoA |
|  |  | 612.9 → 168.9 |  |  |  |  |  |  |  |
| PFTriA | 664 | 662.9 → 618.9 | 0.10 | 12.11 | 0.1 | 0.25 | 5 | 0.991 | MPFDoA |
|  |  | 662.9 → 168.9 |  |  |  |  |  |  |  |
| PFTreA | 714 | 712.9 → 668.9 | 0.10 | 12.61 | 0.5 | 0.5 | 10 | 0.996 | M2PFTeDA |
|  |  | 712.9 → 168.9 |  |  |  |  |  |  |  |
| PFBS | 300 | 298.9 → 80.0 | 0.40 | 7.08 | 0.1 | 0.1 | 2 | 0.999 | M3PFBS |
|  |  | 298.9 → 98.9 |  |  |  |  |  |  |  |
| PFPeS | 350 | 348.9 → 80.0 | 0.60 | 9.14 | 0.5 | 0.5 | 10 | 0.995 | M3PFBS |
|  |  | 348.9 → 98.9 |  |  |  |  |  |  |  |
| PFHxS | 400 | 398.9 → 80.0 | 0.80 | 9.70 | 0.1 | 0.25 | 5 | 0.992 | MPFHxS |
|  |  | 398.9 → 98.9 |  |  |  |  |  |  |  |
| PFHpS | 450 | 448.9 → 80.0 | 0.70 | 10.14 | 0.5 | 0.5 | 10 | 0.994 | MPFOS |
|  |  | 448.9 → 98.9 |  |  |  |  |  |  |  |
| PFOS | 500 | 498.9 → 80.0 | 0.50 | 10.52 | 0.25 | 0.25 | 5 | 0.996 | MPFOS |
|  |  | 498.9 → 98.9 |  |  |  |  |  |  |  |
| PFNS | 550 | 548.9 → 80.0 | 0.60 | 10.89 | 0.1 | 0.1 | 2 | 0.992 | MPFOS |
|  |  | 548.9 → 98.9 |  |  |  |  |  |  |  |
| PFDS | 600 | 598.9 → 80.0 | 0.40 | 11.22 | 0.1 | 0.25 | 5 | 0.994 | MPFOS |
|  |  | 598.9 → 98.9 |  |  |  |  |  |  |  |
| PFOSA | 499 | 497.9 → 78.0 | 0.05 | 11.38 | 0.5 | 0.1 | 2 | 0.995 | M8FOSA-I |
|  |  | 497.9 → 168.9 |  |  |  |  |  |  |  |
| HFPO-DA | 330 | 284.9 → 168.9 | 0.10 | 9.23 | 1.0 | 2.5 | 50 | 0.996 | M3HFPO-DA |
|  |  | 328.9 → 284.9 |  |  |  |  |  |  |  |
| 4:2 FtS | 328 | 326.9 → 306.9 | 0.15 | 8.89 | 0.1 | 0.25 | 5 | 0.993 | M2-4:2FTS |
|  |  | 326.9 → 81.0 |  |  |  |  |  |  |  |
| 6:2 FtS | 428 | 426.9 → 406.9 | 0.15 | 10.15 | 0.1 | 0.1 | 2 | 0.996 | M2-6:2FTS |
|  |  | 426.9 → 81.0 |  |  |  |  |  |  |  |
| 8:2 FtS | 528 | 526.9 → 506.9 | 0.15 | 10.95 | 0.1 | 0.1 | 2 | 0.999 | M2-8:2FTS |
|  |  | 526.9 → 81.0 |  |  |  |  |  |  |  |
| N-MeFOSAA | 571 | 569.9 → 418.9 | 0.40 | 11.13 | 0.1 | 0.1 | 2 | 0.994 | d3-NMeFOSAA |
|  |  | 569.9 → 511.9 |  |  |  |  |  |  |  |
| N-EtFOSAA | 585 | 583.9 → 418.9 | 0.80 | 11.29 | 0.25 | 0.25 | 5 | 0.996 | d5-NEtFOSAA |
|  |  | 583.9 → 525.9 |  |  |  |  |  |  |  |
| ADONA | 378 | 376.9 → 250.9 | 0.15 | 9.77 | 0.1 | 0.1 | 2 | 0.993 | MPFOA |
|  |  | 376.9 → 85.0 |  |  |  |  |  |  |  |
| 9Cl-PF3ONS | 532 | 530.9 → 350.9 | 0.10 | 10.70 | 0.1 | 0.1 | 2 | 0.994 | MPFDA |
|  |  | 530.9 → 83.0 |  |  |  |  |  |  |  |
| 11Cl-PF3OUdS | 630 | 630.9 → 450.9 | 0.05 | 11.39 | 0.1 | 0.1 | 2 | 0.998 | MPFUdA |
|  |  | 630.9 → 83.0 |  |  |  |  |  |  |  |

a: Molecular weight (Da)

b: The first ion transition was used for quantitation, and the second ion transition was used for confirmation

c: Ratio is defined as the response of the confirmation ion transition over the response of the quantitation ion transition; a tolerance range of 50-150% was applied

d: Retention time (min)

e: First calibration standard (µg/L) with a calculated concentration that is 70-130% of the true value with a signal-to-noise ratio greater than 10

f: LOQ (µg/L) calculated using the signal-to-noise ratio, method blank, and weighted calibration curve

g: Method quantitation limit (MQL; µg/L) for aqueous samples with a 25-mL loading volume

h: NIS

# Table S4. LC-MS/MS operational parameters and select method performance metrics for the 23 MPFAS.

| Compound | MW a | Ion transitions b |  | Ratio | RT c | NIS conc. d | EIS spiked mass e |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MPFBA | 218 | 216.9 → 171.9 | - |  | 3.62 | 5 | - |
|  |  | - |  |  |  |  |  |
| M5PFPeA | 269 | 267.9 → 222.9 | - |  | 6.41 | 5 | - |
|  |  | - |  |  |  |  |  |
| MPFHxA | 316 | 314.9 → 269.9 | 0.01 |  | 9.01 | 5 | - |
|  |  | 314.9 → 118.9 |  |  |  |  |  |
| M4PFHpA | 368 | 366.9 → 321.9 | 0.15 |  | 9.71 | - | 5 |
|  |  | 366.9 → 168.9 |  |  |  |  |  |
| MPFOA | 418 | 416.9 → 371.9 | 0.20 |  | 10.15 | 5 | - |
|  |  | 416.9 → 168.9 |  |  |  |  |  |
| M8PFOA | 422 | 420.9 → 375.9 | 0.20 |  | 10.15 | - | 5 |
|  |  | 420.9 → 171.9 |  |  |  |  |  |
| MPFNA | 469 | 467.9 → 422.9 | 0.20 |  | 10.52 | - | 5 |
|  |  | 467.9 → 168.9 |  |  |  |  |  |
| MPFDA | 516 | 514.9 → 469.9 | 0.10 |  | 10.90 | 5 | - |
|  |  | 514.9 → 218.9 |  |  |  |  |  |
| MPFUdA | 566 | 564.9 → 519.9 | 0.05 |  | 11.28 | 5 | - |
|  |  | 564.9 → 168.9 |  |  |  |  |  |
| MPFDoA | 616 | 614.9 → 569.9 | 0.05 |  | 11.67 | - | 5 |
|  |  | 614.9 → 168.9 |  |  |  |  |  |
| M2PFTreA | 716 | 714.9 → 669.9 | 0.10 |  | 12.61 | 5 | - |
|  |  | 714.9 → 168.9 |  |  |  |  |  |
| M3PFBS | 303 | 301.9 → 80.0 | 0.40 |  | 7.11 | 5 | - |
|  |  | 301.9 → 98.9 |  |  |  |  |  |
| MPFHxS | 404 | 402.9 → 84.0 | 0.80 |  | 9.76 | 5 | - |
|  |  | 402.9 → 102.9 |  |  |  |  |  |
| M3PFHxS | 403 | 401.9 → 80.0 | 0.80 |  | 9.75 | - | 5 |
|  |  | 401.9 → 98.9. |  |  |  |  |  |
| MPFOS | 504 | 502.9 → 80.0 | 0.50 |  | 10.52 | 5 | - |
|  |  | 502.9 → 98.9 |  |  |  |  |  |
| M8PFOS | 508 | 506.9 → 80.0 | 0.50 |  | 10.53 | - | 5 |
|  |  | 506.9 → 98.9 |  |  |  |  |  |
| M8FOSA-I | 507 | 505.9 → 78.0 | 0.05 |  | 11.38 | - | 5 |
|  |  | 505.9 → 171.9 |  |  |  |  |  |
| M2-FtS 4:2 | 330 | 328.9 → 308.9 | 0.15 |  | 8.95 | 5 | - |
|  |  | 328.9 → 81.0 |  |  |  |  |  |
| M2-FtS 6:2 | 430 | 428.9 → 408.9 | 0.15 |  | 10.15 | 5 | - |
|  |  | 428.9 → 81.0 |  |  |  |  |  |
| M2-FtS 8:2 | 530 | 528.9 → 508.9 | 0.15 |  | 10.97 | 5 | - |
|  |  | 528.9 → 81.0 |  |  |  |  |  |
| M3HFPO-DA | 333 | 286.9 → 168.9 | 0.15 |  | 9.23 | 25 | - |
|  |  | 331.9 → 286.9 |  |  |  |  |  |
| d3-NMeFOSAA | 574 | 572.9 → 418.9 | 0.40 |  | 11.13 | 5 | - |
|  |  | 569.9 → 514.9 |  |  |  |  |  |
| d5-NEtFOSAA | 590 | 588.9 → 418.9 | 0.80 |  | 11.28 | 5 | 5 |
|  |  | 588.9 → 530.9 |  |  |  |  |  |

a: Molecular weight (Da)

b: The first ion transition was used for quantitation; the second ion transition was used for confirmation

c: Retention time (min)

d: MPFAS concentration (µg/L) when used as NIS

e: Spiked mass of MPFAS (ng) when used as EIS during SPE and solvent extraction

# Table S5. Adsorption isotherm model parameters for PFOS in deionized water and filtered surface water by Ga/TNTs@AC.

| Model | Parameter | Deionized water | Filtered surface water |
| --- | --- | --- | --- |
| Freundlich | KF (mg/g·(L/mg)1/n) | 28.4 | 29.8 |
|  | n | 3.72 | 3.56 |
|  | R2 | 0.99 | 0.96 |
| Langmuir | Qmax (mg/g) | 18.1 | 18.7 |
|  | KL (L/mg) | 137 | 136 |
|  | R2 | 0.96 | 0.98 |

# Table S6. Major cations and other water quality parameters for the filtered surface water after adsorption by Ga/TNTs@AC. All concentrations are reported as mean ± standard deviation.

| Cations | Concentration (mg/L) | Other parameters | Value |
| --- | --- | --- | --- |
| Ca2+ | < 0.1 a | Hardness b | < 0.1 a |
| Mg2+ | < 0.1 a | pH | 7.0 ± 0.1 |
| K+ | 0.10 ± < 0.01 a | TOC c | 1.04 ± 0.6 |
| Na+ | 45.7 ± 0.5 |  |  |

a: Concentration was below the limit of quantitation

b: Hardness in mg/L as CaCO3

c: Total organic carbon in mg-C/L

# Figures

# Figure S1. Map of the study area showing the location of the 3M Guin Facility, Purgatory Creek, and the sampling site.

# Figure S2. The total ion current for a solution containing 10 µg/L of 28 PFAS and 5 µg/L of 23 MPFAS (denoted by blue labels); (b) calibration curves for two representative PFAS with short and long retention times and their validated linear range; and, (c) chromatograms for the same two PFAS showing symmetric peaks.

# Figure S3. Absolute recovery (n = 3; error bars are standard deviation) for 5 ng of PFAS spiked into 25 mL of deionized water and surface water during SPE.

# Figure S4. Kinetics of DOM adsorption to Ga/TNTs@AC in filtered surface water. Experimental conditions: Initial PFOS spiked in FSW = 100 µg/L, Material dosage = 1 g/L, pH = 7.0 ± 0.1, Initial DOM = 3.39 mg/L as TOC. Data are plotted as the mean of duplicates with error bars indicating deviation from the mean.

# Figure S5. Effect of solution pH on photocatalytic degradation of PFOS by Ga/TNTs@AC during UV irradiation. Experimental conditions for adsorption: Initial PFOS spiked in FSW = 100 µg/L, Contact time = 2 h; Material dosage = 3 g/L, Adsorption time = 2 h, and pH = 7.0 ± 0.1. Conditions for photocatalysis: Solid/Solution = 0.12g/10 mL, UV Wavelength = 254 nm, Intensity = 210 W/m2, Irradiation time = 4 h. Data are plotted as the mean of duplicates with error bars indicating relative deviation from the mean.

# Figure S6. Defluorination efficiency of PFOS by Ga/TNTs@AC in the presence of Fe3+after 4 h of UV irradiation. Experimental conditions for adsorption: PFOS spiked in FSW = 100 µg/L; Material dosage = 3 g/L; Contact time = 2 h; pH = 7.0 ± 0.1. Conditions for photocatalysis: Solid/Solution = 0.12g/10 mL; Intensity = 210 W/m2, Irradiation time = 4 h; pH = 3.5 ± 0.2. Data are plotted as the mean of duplicates with error bars indicating relative deviation.

# Figure S7. Effluent pH during a fixed-bed column run using Ga/TNTs@AC. Influent composition: PFOS = 100 µg/L, Ca2+ = 2.03 mg/L, K+ = 1.17 mg/L, Mg2+ = 0.67 mg/L, Na+ = 2.47 mg/L, Cl– = 2.04 mg/L, F– = 0.03 mg/L, NO3– = 1.40 mg/L, and TOC = 3.35 mg/L.

References

Huang, J., Zou, Y. and Ling, L.  2024.  Enhanced selective photocatalytic reduction and oxidation of perfluorooctanoic acid on Bi/Bi5O7I decorated with poly (triazine imide). J. Hazard. Mater. 480, 136257. https://doi.org/10.1016/j.jhazmat.2024.136257

Li, X., Xiao, X., Zhang, S., Teng, X., Wang, Z. and Qu, R.  2025.  Self-regenerable zeolite Beta (35) for efficient adsorption and photocatalytic degradation of PFOA under simulated solar irradiation. Water Research, 124645. https://doi.org/10.1016/j.watres.2025.124645

Li, F., Wei, Z., He, K., Blaney, L., Cheng, X., Xu, T., Liu, W., Zhao, D., 2020. A concentrate-&-destroy technique for degradation of perfluorooctanoic acid in water using a new adsorptive photocatalyst. Water Res., 116219. https://doi.org/10.1016/j.watres.2020.116219.

Liu, F., Guan, X., Xiao, F., 2022. Photodegradation of per-and polyfluoroalkyl substances in water:A review of fundamentals and applications. J. Hazar. Mater. 439, 129580. https://doi.org/10.1016/j.jhazmat.2022.129580.

Liu, W., Cai, Z.Q., Zhao, X., Wang, T., Li, F., Zhao, D.Y., 2016. High-capacity and photoregenerable composite material for efficient adsorption and degradation of phenanthrene in water. Environ. Sci. Technol. 50(20), 11174-11183. https://doi.org/10.1021/acs.est.6b02623.

U.S. Environmental Protection Agency (EPA). 2024. Analysis of per- and polyfluoroalkyl substances (PFAS) in aqueous, solid, biosolids, and tissue samples by LC-MS/MS. https://www.epa.gov/system/files/documents/2024-12/method-1633a-december-5-2024-508-compliant.pdf

Zhu, Y., Xu, T., Zhao, D., Li, F., Liu, W., Wang, B., An, B., 2021. Adsorption and solid-phase photocatalytic degradation of perfluorooctane sulfonate in water using gallium-doped carbon-modified titanate nanotubes. Chem. Eng. J. 421, 129676. https://doi.org/10.1016/j.cej.2021.129676.

Zhu, Y., Ji, H., He, K., Blaney, L., Xu, T., Zhao, D. 2022. Photocatalytic degradation of GenX in water using a new adsorptive photocatalyst. Water Res. 220, 118650. https://doi.org/10.1016/j.watres.2022.118650.