Supplemental Information for:

Uptake Mechanisms of a Novel, Activated Carbon-Based Equilibrium Passive Sampler for Estimating Porewater Methylmercury

The Supporting Information includes an unabridged methods section, additional discussion sections, 10 figures, and 9 tables.

SI 1. Materials and Methods

SI 1.1 Production of ag+AC polymer samplers

The ag+AC polymers were produced using a virgin powdered AC derived from bituminous coal (Calgon Type 3055; 80 x 325 TOG LF; C(%) = 80.9±1.4; surface area = 1116±25 m2/g; skeletal density = 1.61 g/cm3; bulk density = 0.64 g/cm3). AC particles were sieved to >53μm, then washed with DI and allowed to dry in a 30 °C oven prior to casting within gels or indirect experimental use to ensure uniformity. Following the preparation methods described in detail in Sanders et al.,2020, 0.300 g of prepared dry PAC was mixed with 0.300 g of agarose powder, then 20 mL of DI water was added, and the solution was stirred while heated in a hot water bath for 4.5 mins. Across all experiments, ag+AC polymers were prepared identically to a uniform thickness (1 mm) by casting the agarose gel suspension between two acid-cleaned glass plates separated by spacers (Gao et al., 2011; Gomez-Eyles et al., 2013; Sanders et al., 2020). Gels were allowed to cool for 1 hour, then cut to a uniform size of 34.3 mm by 23.9 mm and stored in clean DI water until use. The gel was sufficiently rigid that transfer between experimental bottles was accomplished using acid-cleaned forceps to gently transfer samplers.

SI 1.2 MeHgCys Sorption Isotherms

Partitioning of MeHg complexed with L-Cysteine was evaluated for both the ag+AC passive samplers and bare AC particles. Isotherm solutions were spiked with a MeHgCl standard (Brooks Rand Laboratories) diluted to five concentrations ranging from 3 to 300 ng/L (bare AC particles) or 30 to 3000 ng/L (ag+AC polymers). All experimental isotherms were conducted in 60-mL polyethylene terephthalate glycol (PETG) copolymer bottles. L-cysteine (Sigma-Aldrich, 98%) was added to each experimental bottle to maintain a 105:1 molar ratio of L-cysteine to MeHg, and buffered with the addition of 1mM MOPS (3-Morpholinopropane-1-sulfonic acid). Solutions were incubated overnight in the dark on a shaker table at 60 rpm at 4 °C prior to sampler addition to ensure a stable MeHg distribution. Samplers or ~0.010g of bare AC particles were added to experimental bottles in triplicate at each concentration level., and were allowed to equilibrate for 14 days in the dark on a shaker table at 60 rpm at 4 °C. After 14 days, ag+AC samplers were carefully removed with forceps, and bare AC particles were separated from overlying solution with centrifugation followed by careful pipetting. After separation, sorbents were stored frozen. A portion of the overlying water was acidified to 0.5% v/v with trace metal grade HCl to preserve MeHg, then stored refrigerated at 4 °C. Aliquots of overlying water after 14 days were taken from one treatment of each triplicate to evaluate pH and sulfide concentration within the experimental solutions to monitor for cysteine degradation. All solutions were below detection limit (BDL) for sulfide. DI water blanks and control bottles containing the sorbents and the cysteine solution without a MeHg spike were processed in tandem with the experimental samples. All blanks and controls exhibited negligible amounts of MeHg.

SI 1.3 DOM Sorption Isotherm Experiments

Partitioning of MeHgDOM species to the ag+AC polymer material was evaluated for seven different organic matter sources with varying characteristics (summarized in Table S5; all obtained from the International Humic Substances Society) in an isotherm experiments. All MeHgDOM species were prepared by adding MeHgCl stock to a saline (3 ppt Instant Ocean, United Pet Group, Inc.) solution containing 7.5 mM NaHCO3 (Avantor Macron Fine Chemicals) to buffer pH (8.2-8.7) at near-neutral condition. MeHgCl spiked DOM solutions were incubated in the dark on a shaker table at 60 rpm at 4 °C for a minimum of 24 hours to ensure a stable MeHg distribution at high affinity sites within the DOM complexes. Saline experimental solution conditions were chosen to set a consistent ionic strength across experimental treatments with varying parameters.

Isotherms (referred to as “varying ratio DOM isotherms”) were conducted with DOC concentrations held constant at 5 mg/L across the range of initial MeHg concentrations ranging from 5 to 330 ng/L, resulting in DOM:MeHg mass ratios ranging from 106:1 to 1.5×104:1. This approach was used to avoid potential saturation of the passive sampler AC with DOM molecules. For these isotherms, one ag+AC sampler was added to an experimental bottle containing the DOM stock but without a MeHgCl spike to evaluate DOM partitioning in the absence of MeHg (ag+AC DOC blank). DOM-containing blanks and MeHg controls (at an initial MeHg spike of ~50 ng/L) for each DOM source were processed in tandem with the ag+AC sampler treatments.

ag+AC samplers were added to each PETG bottle, and were incubated in the dark on a shaker table at 60 rpm at 4 °C. After 14 days, ag+AC samplers were carefully removed with acid cleaned forceps. Aliquots of overlying water were removed from each bottle to evaluate pH, DOC concentration, and sulfide concentration within the experimental solutions. All solutions were BDL for sulfide. All blanks exhibited negligible amounts of MeHg, and controls displayed insignificant degradation of MeHg over the 14-day incubation period.

SI 1.4 Isotopically-Labelled Experiments to Verify Equilibrium Exchange Behavior

SI 1.4.1 Isotopically-Labelled MeHgSRHA Experiments

A series of experiments were conducted to explicitly verify the equilibrium exchange of MeHg by the ag+AC samplers, utilizing isotopically-labelled MeHg species to track exchange over 14-day time courses. To evaluate the exchange of MeHg between an environmentally relevant MeHg species and the ag+AC polymer material, a solution containing 5 mg/L of Suwannee River Humic Acid (SRHA III, IHSS) was prepared. To this SRHA solution, aliquots of either Me198HgCl or Me199HgCl were added to create solutions at a nominal concentration of 50 ng/L. SRHA was chosen as the DOM source for the exchange experiments due to the availability of published data to estimate the number of thiolic sites (Poulin et al., 2017). Solutions were incubated overnight in the dark on a shaker table at 60 rpm at 4 °C prior to sampler addition to ensure a stable MeHgSRHA distribution. Samplers were added to experimental bottles containing Me199HgSRHA in duplicate, then allowed to equilibrate for 14 days in the dark on a shaker table at 60 rpm at 4 °C. To evaluate uptake of Me199HgSRHA, after 14 days 2 bottles containing bare AC particles and two containing ag+AC samplers were separated as described in detail in Section S1.2.

After the 14-day equilibration period, ag+AC samplers were carefully removed with acid-cleaned forceps and transferred to experimental bottles containing Me198HgSRHA. The same general procedure was followed for bare AC particles, with the following exceptions: equilibration time was only 48 hours, transfer of bare AC particles involved separation from Me199HgSRHA solution by centrifugation followed by careful pipetting, and washing of the centrifuge tubes with Me198HgSRHA solutions to ensure complete mass transfer. Transfer of Me199HgSRHA solution to bottles containing Me198HgSRHA solutions was minimal (<<0.5mL) for both transfer methods. After transfer, experimental bottles were again placed onto a shaker table at 60 rpm at 4 °C in the dark. Experimental bottles were removed, separated, and preserved in duplicate over a time course to observe exchange of the isotopically-labeled MeXXXHgSRHA species. Bottles containing bare AC particles were removed after 0.25, 1, 3, 6, 24, and 48 hours, while ag+AC containing bottles were removed after 1, 6, 24, 48, 168, and 336 hours.

In tandem with experimental solutions, bottles containing blank and control solutions of both MeXXXHgSRHA species were prepared. Control solutions were preserved for analysis at the start and end of both the uptake and exchange phases. SRHA blanks were negligible for MeHg, and control solutions indicated that there was minimal degradation of MeHgSRHA species over the experiment duration.

SI 1.4.2 Isotopically-Labelled MeHgCys Exchange Experiments

This experiment was designed to mimic the previous dual isotope label experiment, but using MeHgCys as the dominant species instead of MeHgSRHA. For both experimental phases (uptake and exchange) a solution was prepared to contain cysteine at a nominal concentration of 2.5E-5 M along with 7.5 mM bicarbonate and 3ppt Instant Ocean. The cysteine concentration was determined such that a 105:1 molar ratio of cysteine to MeXXXHg would be maintained, mimicking the cysteine sorption isotherm experiments. However, concentrations of the two isotope spikes ended up being lower than anticipated in initial experimental solutions (Me199HgCys = 8.75 ng/L, Me198HgCys = 17 ng/L), resulting in actual molar ratios closer to 5×105:1. Samplers were allowed to equilibrate with the exchange phase solution containing Me199HgCys for 14 days on a shaker table at 60 rpm at 4 C in the dark, then carefully transferred to new PETG bottles containing the Me198HgCys solution. Samplers were removed in triplicate at the following times: 1 hr, 6 hr, 24 hr, 48 hr, 96 hr, 7 days, 14 d, with an additional 3 samplers preserved prior to insertion in the exchange phase solution during the switchover process to evaluate Me199HgCys uptake. Experimental blanks exhibited negligible MeHg, and control bottles for both Me199HgCys and Me198HgCys exhibited minimal degradation over the respective 14-day equilibration periods.

SI 1.4.3 Isotopically-Labelled MeHgCys & MeHgSRHA Release Experiments

Two additional exchange experiments were conducted to evaluate the exchange dynamics of MeHg species at equilibrium with the passive sampling polymer when exposed to an aqueous solution containing differing environmentally-relevant high MeHg affinity ligands. Both uptake and exchange solutions were saline and buffered to near neutral pH (3 ppt Instant Ocean and 7.5 mM sodium bicarbonate). One set of polymers was allowed to equilibrate with Me199HgCys during the 14-day uptake phase and transferred to a solution containing SRHA for the exchange phase, and separate set of polymers equilibrated with Me199HgSRHA during uptake and transferred to an exchange solution containing cysteine. The exchange solutions (cysteine at 2.5E-5 M conc., and SRHA at 10 mg/L DOC) for these two experimental treatments were prepared without a MeHg spike to prevent isotopic exchange between ligand-bearing species during the exchange phase that might obfuscate sampler:water MeHg partitioning. Samplers were removed in duplicate at the following times for each experimental treatment: 1 hr, 6 hr, 24 hr, 48 hr, 96 hr, 7 days, 14 d, with 2 additional samplers preserved prior to insertion in the exchange phase solutions to evaluate either Me199HgCys or Me199HgSRHA uptake. Solution blanks for all phases were negligible for MeHg, and uptake phase MeHg control bottles exhibited minimal degradation. DOC concentrations were measured in overlying waters for the Me199HgSRHA uptake phase bottles, and in the overlying waters of both exchange phase solutions.

SI 1.4.4 Kinetic Modelling of Isotopically-Labelled Exchange Experiment

The timeseries data to the dual-isotopic exchange experiments using MeHgSRHA and MeHgCys were each fitted to a model following first order kinetics with equilibrium exchange under finite volume batch conditions simulating the experimental conditions. The first order kinetic coefficients for adsorption of Me198Hg, kadsorb, and desorption of Me199Hg, kdesorb, were calculated independently. Likewise, the time it takes for the system to reach 90% equilibrium under experimental conditions was calculated for each isotopic species.

The sampler concentrations through time were fitted to a first order kinetic model with equilibrium exchange, shown in Equation 1,

|  | dCps,tdt=-k∙Cps,t-Cps,eq | (1) |
| --- | --- | --- |

where Cps,t [ng/kg] is the sampler concentration at time t (d), k (d-1) is the kinetic coefficient describing adsorption, and Cps,eq is the sampler concentration at equilibrium with the water concentration at time t. This kinetic equation was used to model the desorption of the preloaded Me199Hg and the adsorption of Me198Hg, independently. The (Cps,t – Cps,eq) term represents the concentration gradient driving the shift towards equilibrium. Using the equilibrium partitioning relationship, Cps,eq can thus be replaced with the product of the concentration in the water at time t multiplied by the equilibrium partitioning coefficient, Cw,tKps, as in Equation 2.

|  | dCps,tdt=-k∙Cps,t-Cw,tKps | (2) |
| --- | --- | --- |

Kps [L/kg] was calculated as the overall Cps,t/Cw,t ratio at the final 14-day timepoint, inclusive of both isotopic species; log Kps = 1.26 was used for the experiments using MeHgSRHA and log Kps = 3.54 was used for experiments using MeHgCys. Cw,t is related to Cps,t via the following mass balance equation for Me199Hg,

|  | 199Cw,t= 199Cps,0mps- 199Cps,tmpsVw | (3) |
| --- | --- | --- |

where mps is the mass of the sampler [kg], Vw is the volume of the exchange solution [L], and 199Cps,0 is the initial Me199Hg concentration in the sampler (ng/kg), which was estimated under the assumption that the entire mass of Me199Hg was initially present in the preloaded sampler. Substituting 199Cw,t into Equation 2,

|  | d 199Cps,tdt=-k∙ 199Cps,t-KpsmpsVw( 199Cps,0- 199Cps,t) | (4) |
| --- | --- | --- |

expanding,

|  | d 199Cps,tdt=-k∙(1+KpsmpsVw) 199Cps,t-KpsmpsVw 199Cps,0 | (5) |
| --- | --- | --- |

reducing constant terms (1 + Kpsmps/Vw) to constant a, and term Kpsmps199Cps,0/Vw to constant b,

|  | d 199Cps,tdt=-k∙a 199Cps,t-b | (6) |
| --- | --- | --- |

then isolating 199Cps,t yields the following.

|  | d 199Cps,tdt=-ka∙ 199Cps,t-ba | (7) |
| --- | --- | --- |

Separating variables,

|  | d 199Cps,t 199Cps,t-ba=-ka dt | (8) |
| --- | --- | --- |

then integrating leads to the following solution,

|  | ln 199Cps,t-ba=-kat+Q | (9) |
| --- | --- | --- |

where Q is an undefined constant. Rearranging,

|  | 199Cps,t-ba=Q exp⁡(-kat) | (10) |
| --- | --- | --- |

Q is solved by substituting Cps,0 for Cps,t at t = 0 as such.

|  | 199Cps,0-ba=Q exp⁡(-kat) | (11) |
| --- | --- | --- |

Plugging Q back into the solved equation and isolating 199Cps,t yields the final solution for Me199Hg.

|  | 199Cps,t= 199Cps,0-baexp-kat+ba | (12) |
| --- | --- | --- |

A similar approach is taken for Me198Hg. 198Cw,t is defined with the following mass balance equation,

| 198Cw,t= 198Cw,0Vw- 198Cps,tmpsVw | (13) |
| --- | --- |

where 198Cw,0 is the initial concentration of Me198Hg in the exchange solution (ng/L). 198Cw,0 was estimated using data at each timepoint by assuming the entire Me198Hg mass in the system at time t was initially present in the solution. Substituting 198Cw,t into Equation 2,

|  | d 198Cps,tdt=-k∙ 198Cps,t-KpsVw 198Cw,0Vw- 198Cps,tmps | (14) |
| --- | --- | --- |

then rearranging yields the following.

|  | d 198Cps,tdt=-k∙(1+KpsmpsVw) 198Cps,t-Kps 198Cw,0 | (15) |
| --- | --- | --- |

Reducing the term (1 + Kpsmps/Vw) to constant a (as the with Me199Hg equation) and the term Kps198Cw,0 to constant d,

|  | d 198Cps,tdt=-k∙a 198Cps,t-d | (16) |
| --- | --- | --- |

and isolating 198Cps,t gives the following.

|  | d 198Cps,tdt=-ka∙ 198Cps,t-da | (17) |
| --- | --- | --- |

Separating variables,

|  | d 198Cps,t 198Cps,t-da=-ka dt | (18) |
| --- | --- | --- |

then integrating yields the following solution,

|  | ln 198Cps,t-da=-kat+S | (19) |
| --- | --- | --- |

where S is an undefined constant. Transforming,

|  | 198Cps,t-da=S exp⁡(-kat) | (20) |
| --- | --- | --- |

S is solved by substituting 0 for 198Cps,t at t = 0 as such,

|  | -da=S exp⁡(-kat) | (21) |
| --- | --- | --- |

Plugging S back into the solved equation and isolating 198Cps,t yields the final solution for Me198Hg.

|  | 198Cps,t=da1-exp-kat | (22) |
| --- | --- | --- |

The kinetic coefficient k was estimated by iterating its value to maximize the coefficient of determination, R2, between the estimated and measured sampler concentrations. A model dataset was built using the obtained k values with the average Cps,0, Cw,0, and mps. The model is plotted with the experimental data in Figures S6a and S6b.

It should be noted that the measured initial and final Me199HgCys concentrations were indistinguishable (t-test, α = 0.05), so it is hard to visibly see the desorption of Me199HgCys in Figure S6B. Despite this minor change over time, the first order model provides a good fit for this dataset, and the kinetic coefficient k is similar to that of Me198HgCys.

The estimated time for the system to reach 90% equilibrium conditions was calculated by using Equations 12 and 22 to solve for t at the Cps,t90 defined by Equation 23.

|  | Cps,t90=Cps,0-0.9∙Cps,0-Cps,eq | (23) |
| --- | --- | --- |

where

|  | 199Cps,eq= 199Cps,0mpsmps+VwKps | (24) |
| --- | --- | --- |

and

|  | 198Cps,eq= 198Cw,0Vwmps+VwKps | (25) |
| --- | --- | --- |

The average Cps,0, Cw,0, and mps were used to estimate t90.

SI 1.5 Microcosm Experiments to Determine Passive Sampler Predictive Capability in Sediment and Water

As an initial demonstration of the potential field applications of this passive sampling polymer, a sediment microcosm experiment was conducted to determine to a first order the ability of the ag+AC samplers to predict in situ MeHg concentrations in sediment and overlying water. To mimic a moderately contaminated marsh soil (target 10 ppm total Hg), a mixture of soil from an oligohaline Phragmites australis marsh in Berry’s Creek, NJ, and a Phragmites australis marsh soil from the Smithsonian Environmental Research Center (SERC) Global Change Research wetland in Edgewater, MD was utilized. Prior to the study, this soil mixture had been used in a 18 month field mesocosm experiment in a tidal creek at SERC (Schwartz, unpublished data). Soils collected after the mesocosm study were stored at 4 °C for an additional 26 months prior to the current experiment. Immediately prior to the passive sampler experiment, measured MeHg concentration in the mixture was 19.5 ng/g wet soil. The mixture was thoroughly homogenized via paint mixer, after which 100 g of the wet soil mixture was placed into 500 mL glass jars. Artificial salt water (100 mL of 3 ppt Instant Ocean) was gently added on top of the soil layer. The microcosms were loosely capped and gently aerated at a constant rate throughout the experiment. Microcosms were allowed to equilibrate for 14 days prior to sampler insertion to allow development of redox gradients in the soil mixture.

Two configurations of passive samplers were tested; one in which separate samplers were deployed in water and sediment, and another in which a single sampler was deployed across the sediment/water interface. Full-size samplers deployed across the sediment-water interface were synthesized as described in Section 2.1. These full-size samplers (referred to throughout as “sheet-ps”), were inserted across the sediment-water interface at a slight incline (Figure S8), such that half of the sampler mass was located in the sediment while the other half remained in the water column. To provide rigidity, the ag+AC samplers were heat sealed in acid cleaned polypropylene mesh (McMaster Carr, 0.21mm mesh) prior to insertion in the microcosms.

Half-sized samplers (17.2 mm by 23.9 mm) denoted as “split-ps,” were deployed separately in sediment and water in a different set of microcosms to evaluate whether there was significant vertical diffusion of MeHg species within the agarose matrix of the samplers. The sampler inserted in the sediment was tied to the sampler in the water with acid-cleaned nylon thread to anchor the sampler suspended in the water column. The sediment sampler was inserted at a slight incline into the sediment, while the water sampler was fully submerged within the overlying water. Microcosms without samplers (referred to as “no-ps”) served as controls to help evaluate any effects that the samplers may have on the sediment porewater chemistry or native MeHg concentration through time. The sheet-ps and split-ps pairs were deployed individually in separate microcosms, and the no-ps, sheet-ps, and split-ps microcosm configurations were constructed in triplicate.

At each experimental time point, passive samplers, overlying water, porewater, and sediment were collected from the microcosms for further analysis. The sheet-ps and split-ps microcosms were sampled 14 and 21 days after sampler insertion (t+14 and t+21, respectively), with an additional sheet-ps microcosm take down 7 days after insertion (t+7). Upon removal, the sheet-ps and split-ps were gently rinsed with DI water to remove sediment particles. Sediment (ps-sed) and overlying water (water-ps) portions of split-ps samplers were separated by cutting the connecting nylon thread. Sheet-ps samplers were split at the visually determined soil-water interface with clean, DI-rinsed shears, then frozen until analysis. Sacrificial no-ps microcosms were sampled hours after microcosm construction (t-14), at sampler insertion (t+0), and at each sampler retrieval date (t+7, t+14, and t+21). A sacrificial beaker filled with DI water was deployed alongside the microcosm, from which water was taken at the t0, t+7, t+14, and t+21 timepoint as a quality control blank. A passive sampler was deployed in this beaker and retrieved at t+21 for the same purpose.

At each experimental time point, overlying water was carefully pipetted from the microcosm. Subsequent handling of the sediment and porewater was performed in an anaerobic glove bag (Coy ©, Ann Arbor, MI) to maintain redox conditions after extraction. The bag was filled with 95% N2:5% H2. Anaerobic conditions were maintained with a Pd catalyst system to remove O2. The remaining wet sediment was centrifuged to separate out the porewater, which was then decanted with a pipette. Both overlying- and pore- waters were filtered with a 0.45 μm glass microfiber syringe filter into clean 60mL PETG bottles, from which aliquots were taken for analysis of sulfide, pH, anions, and DOC. Filtrates were then preserved with 0.5% HCl and stored at 4 °C prior to MeHg analysis. An aliquot of the centrifuged sediment was frozen and then lyophilized prior to MeHg analysis.

Effects within the microcosm study were analyzed using standard least squares models that considered time, sampler type, and sampler placement with an overall  =0.05. Parameters were transformed as needed to approximate normal distribution.

SI 1.6 Analytical Methods

For all samples, MeHg was measured by isotope dilution mass spectrometry after separation by acid distillation, following the method detailed in Gilmour et al., 2013, using an Agilent 7900 ICP-MS and Brooks-Rand MERX MeHg analysis system. One adjustment was made to the distillation protocol described in Mitchell and Gilmour, 2008 and Hollwegg et al 2009, with 1% APDC (ammonium pyrrolidine dithiocarbamate, Acros Organics) replacing CuSO4 as the main complexation agent in the distillation matrix as described in EPA Method 1630, (1998 ed.), as this was found to improve isotope dilution spike recovery for samples containing AC particles (EPA Method 1630, 1998 ed.). Me199Hg isotope dilution standards were synthesized in-house (Bancon-Montigny et al., 2004) and checked for concentration and degradation by comparing SnCl2-reducible Hg concentrations before and after BrCl digestion (De Wild et al., 2002). MeHg standards and dilutions were maintained in 0.1% (v/v) TMG HCl and 0.5 % (v/v) acetate buffer, and stored in the dark at 4 °C. For all experiments described in this manuscript, MeHg mass balance was maintained throughout the duration of the experiments. MeHg quality assurance data are summarized in Table S4. Throughout the manuscript, log(Kps) values for the ag+AC passive samplers are reported according to Equation (26):

(26)	log(Kps) = log10(Cps/Cw)

Where Cps is the MeHg concentration (ng MeHg/kg of wet polymer material) measured within the ag+AC polymer and cw is the MeHg concentration (ng of MeHg/L) of the overlying water for a given experiment.

Sulfide was measured by mixing samples 1:1 with sulfide antioxidant buffer (2.0 M NaOH, 0.2 M ascorbic acid, and 0.2 M Na2EDTA in deoxygenated, deionized water prepared anaerobically) and analyzing with a sulfide ion-selective electrode calibrated by lead titration of a saturated sulfide standard. DOC was measured on a Shimadzu TOC-V organic carbon analyzer.

SI 2.1 Additional Discussion of the Partitioning Behavior of Various MeHgDOM Species as Determined from Sorption Isotherms

To test the idea that MeHgDOM partitioning to our samplers reflects the equilibrium of DOM with AC in the samplers (rather than a direct equilibrium between AC and MeHg), we measured DOM sorption to the samplers directly for comparison at a single DOC concentration. The test was done as part of the MeHgDOM isotherm experiments at a varying MeHg:DOM ratios, with partitioning estimated based on the change in aqueous DOC concentration in the experimental solutions over 14 days for a solution without added MeHg spike. Estimated DOM partitioning to the samplers was indeed similar to MeHg partitioning, with log(Kps) values for MeHg from the varying-MeHg:DOM-ratio isotherms displaying a positive correlation with estimated DOM partitioning, although this correlation is insignificant at the α=0.05 level (p=0.09).

One additional isotherm that was not discussed in the main text was conducted under the varying MeHg:DOM mass ratios with SRHA, but for this isotherm the experimental solution contained no Instant Ocean or sodium bicarbonate buffer, which resulted in a lower ionic strength and pH (4.2 instead of 8.4). Although MeHg partitioning did not appear to be depressed in this treatment compared to the buffered treatment (log(Kps) = 2.00±0.80, R2 = 0.76; compared to log(Kps) = 1.98±0.03), the highest MeHg concentration point appears to be driving this apparent high partitioning, as it is the only point that diverges from linear behavior. Without this data point, the linear regression results in a log(Kps) = 0.95 with an R2 = 0.99. As this experiment was not conducted at any level of replication, it is difficult to determine whether the partitioning observed at the highest MeHg concentration is spurious. Partitioning of DOC to the passive sampler was depressed in this isotherm compared to the SRHA isotherm conducted in an aqueous solution containing Instant Ocean and sodium bicarbonate (log(KDOC)= 1.02 compared to log(KDOC)= 1.62, respectively). Previous research has suggested that changes in pH, ionic strength, and DOM concentration all likely affect the macromolecular structure of DOM aggregates, and such changes would fundamentally alter the DOM-AC interactions (Schreiber et al., 2007). Decreased DOM partitioning driven by changes in the pH or ionic strength was likely responsible for decreased MeHg partitioning. A similar depression of partitioning coefficients in lower pH and ionic strengths solutions was also observed in the isotopically labelled MeHgCys exchange experiments. Overall partitioning of MeHgCys to the ag+AC material (log(Kps) 3.540.14 at 14 d) was greater than what was observed during the cysteine isotherm experiment (log(Kps) = 3.010.23), a difference that is likely driven by the differing experimental conditions between the isotherm and exchange experiments, with the isotherms conducted at lower pH and ionic strength. A thorough understanding of the role both pH and ionic strength play in the partitioning of MeHg to AC particles will be critical for extending the use of these passive samplers to a wide range of porewater environments and may have implications for the efficacy of AC as a remediation strategy.

SI 2.2 Additional Discussion of Equilibrium Exchange Experiments with Changing MeHg Speciation

In the exchange experiment with passive samplers initially equilibrated with Me199HgCys and transferred into a solution containing SRHA, Me199Hg concentrations were observed to decrease in the ag+AC polymers and rise correspondingly in the overlying water over the 14 day time course (Fig. S5, Table S6). DOC concentrations fell in the overlying water throughout the 14-day time course (from 9.4 mg/L to 5.6 mg/L DOC), suggesting active partitioning of SRHA to the AC particles. At the end of the exchange phase, log(Kps) = 2.41 for Me199Hg, elevated above the log(Kps) value observed in the SRHA isotherms (log(Kps) = 1.98), but below the previously measured log(Kps) = 3.01± 0.23 observed in the Cys isotherms. This elevated partitioning could be the result of a number of potential scenarios. First, it may reflect a slower exchange of MeHg between passive sampler and overlying water due to the additional interaction of MeHg ligand exchange onto high affinity sites within the organic matter, such that true equilibrium conditions were not met within the 14-day timeframe. It is also possible that larger organic molecules functioned as a physical barrier that prevented efficient release of the relatively smaller MeHgCys molecules from the pore spaces of the AC particles, again resulting in non-equilibrium at the 14-day sampling timepoint.

For the experiment with initial equilibration of the samplers with Me199HgSRHA and subsequent transfer into a solution containing cysteine, Me199Hg concentrations remained relatively constant in both the passive samplers and water (although there is only data for Me199Hg concentrations in the water for timepoints at 48 h, 7 d, and 14 d) (Fig. S5, Table S6). MeHg partitioning is stable for the portion of the time course for which data are available at log(Kps) = 3.24 to 3.17, slightly lower than observed in the MeHgCys:MeHgCys exchange experiments (log(Kps) = 3.54 ± 0.14), but within the error of the partitioning as determined in the cysteine isotherm experiments (log(Kps) = 3.01 ± 0.23). The observed Kps value is higher than observed in the MeHgSHRA:MeHgSHRA exchange experiments (log(Kps) = 1.98). DOC concentrations mirrored MeHg concentrations in the overlying water during the exchange phase in that they were largely invariant over time (0.88 mg/L DOC at 1 hr and 0.89 mg/L at 14 days), and these concentrations were in good agreement with the estimated amount of DOC in solution that would be contributed by cysteine in the initial soluiton prior to passive sampler insertion (0.90 mg/L). Following the proposed equilibration processes, partitioning of MeHg onto the passive sampler material responded to the dominant ligand in solution, in this case cysteine, as demonstrated by the log(Kps) values in good agreement with the cysteine isotherm experiments.

SI 2.3 Additional Discussion of the Sediment Microcosm Experiment

The elevated average MeHg concentration observed in the t+21 split-ps sediment sampler compared to both the t+14 split-ps and the t+21 sheet-ps samplers could reflect changes in a number of factors, including the amount or character of the organic matter within these particular microcosms, potentially altering the partitioning behavior of MeHg. At t+21, the DOC concentrations in the porewater and overlying water of the split-ps treatment were significantly lower than in the sheet-ps treatment, suggesting degradation of organic matter could have contributed to this difference in MeHg uptake between sampler types.

MeHg concentrations in the ag+AC passive sampler portions that were deployed within the overlying water can also be used to predict MeHg Cw. Generally, predictions were less accurate for Cw than they were for Cpw when using log (Kps) values of 2.96 and 3.41, particularly at the t+14 timepoint (Fig. S7). Using the log (Kps) values for MeHgNOM provided a more accurate prediction of Cw at both timepoints, within a factor 3 at t+14 and within a factor of 2 at t+21 for both sampler types. The empirically derived partitioning coefficient (log (Kps) = 3.41) provided poor predictions at both t+14 (within a factor of 7) and t+21 timepoints (within a factor of 6), suggesting that the presence of μM amounts of sulfide and elevated DOC concentrations within the porewaters of the sediment microcosms are impacting the partitioning of MeHg to the ag+AC samplers, likely due to differences in MeHg speciation driven by the presence of sulfide.

Supplemental Figures

Figure S1

Sediment microcosm displaying a sheet-ps sampler inserted across the sediment-water interface.

Figure S2

Exchange of isotopically labelled MeHgSRHA from bare AC particles (CAC-coal) over a 2-d time course. AC particles that had been equilibrated with Me199HgSRHA (orange circles) during an initial 2-d uptake period were transferred to experimental bottles containing Me198HgSRHA (green diamonds), and exchange of these species was observed in both the AC particle sorbents (panel A), and overlying water (panel B). At each timepoint, error bars represent ±1 standard deviation of duplicates. Apparent partitioning coefficients (Cps/Cw) for each isotopically labeled species and for total MeHg (black squares) are shown in panel C.

Figure S3

Exchange of isotopically labelled Me199HgCys from an ag+AC polymer placed in a solution containing Me198HgCys over a 14-d time course. Polymers that had been equilibrated with Me199HgCys (orange circles) during an initial 14-d uptake period were transferred to experimental bottles containing Me198HgCys (green diamonds), and exchange of these species was observed in both the polymer materials (panel A), and overlying water (panel B). At each timepoint, error bars represent ±1 standard deviation of duplicates. Where error bars are not visible, error associated with that timepoint is smaller than the symbol size. Apparent partitioning coefficients (Cps/Cw) for each isotopically labeled species and for total MeHg (black squares) are shown in panel C.

Figure S4

Exchange of isotopically labelled Me199HgCys from an ag+AC polymer in an SRHA solution without MeHg over a 14-d time course. Polymers that had been equilibrated with Me199HgCys (orange circles) during an initial 14-d uptake period were transferred to experimental bottles containing SRHA in solution, and desorption from the polymer, as well as exchange of MeHg between these species, were observed in both the polymer materials (panel A) and overlying water (panel B). DOC concentrations in overlying water are shown in blue squares (B). At a given timepoint, error bars represent ±1 standard deviation of duplicates. Where error bars are not visible, error associated with that timepoint is smaller than the symbol size. Apparent partitioning coefficients (Cps/Cw) for Me199HgCys and organic matter are shown in panel C.

Figure S5

Exchange of isotopically-labelled Me199HgSRHA from an ag+AC polymer in a L-Cysteine containing solution without any MeHg over a 14-day time course. Polymers that had been equilibrated with Me199HgSRHA (orange circles) during an initial 14-d uptake period were transferred to experimental bottles containing L-Cys, and desorption from the polymer, as well as exchange of MeHg between these species was observed in both the polymer materials (panel A), and overlying water (panel B). DOC concentrations of overlying water are shown in blue squares (B). At a given timepoint, error bars represent ±1 standard deviation of duplicates. Where error bars are not visible, error associated with that timepoint is smaller than the symbol size. Apparent partitioning coefficients (Cps/Cw) for Me199HgCys are shown in panel C.

Figure S6

Time series data and first order kinetic model for MeHgSRHA dual-isotopic exchange isotherms (A) and MeHgCys dual-isotopic exchange isotherms (B). Data points represent average values of measured concentrations and error bars represent 1 SD.

Figure S7

Sediment, water and porewater chemistry over time in sediment/water microcosms. Bars show average ± 1 standard deviation for triplicate microcosms at each time point. Colored bars represent three treatments, no passive sampler (green), sheet-ps (blue) or split-ps (orange). For sediment porewater and passive sampler measurements, microcosms were sacrificed at each time point. Sediment and porewater samples were processed under anaerobic conditions.

Fig. S7A. Surface and porewater pH.

Fig. S7B. DOC concentrations in porewater, but not surface water declined significantly over time. For days 14 and 21, DOC levels were lower in microcosms (porewater and surface water) with passive samplers than those without (p<0.003).

Fig. S7C. Chloride in surface and porewater.

Fig. S7D. Sulfate in surface and porewater. There was no significant sulfate depletion through time, or depletion in porewaters relative to surface waters, suggesting limited microbial sulfate reducing activity. Across the last three sampling dates, sulfate in both porewaters and surface waters was higher in the presence of samplers (n=20, p<0.046).

Fig. S7E. Porewater sulfide. Sulfide in porewaters was low (1-4 M) but detectable at all time points. There was no change in porewater sulfide over time. The presence of samplers did not affect porewater sulfide concentrations. There was no detectable sulfide in microcosm surface waters (DL = 0.5 M).

Fig. S7F. MeHg in microcosm surface water (A), porewater (B), sediment (C), and sediment:water MeHg partitioning (D). By days 14 and 21, water column MeHg concentrations were slightly (~25%) but significantly less in the beakers that contained passive samplers than those without (two-way ANOVA on sampling date and presence of sampler, p<0.007). There were no significant differences in porewater MeHg when passive samplers were present. Sediment MeHg concentrations did not change over time, nor were they impacted by the presence of the samplers.

Figure S8

A comparison of aqueous MeHg concentrations with MeHg accumulation by ag+AC samplers. Mean overlying water and porewater MeHg concentrations at (A) 14 days after sampler insertion and (B) 21 days after sampler insertion (left panel). Error bars depict one standard deviation. MeHg concentrations in ag+AC samplers inserted in the sediment and suspended in water, (A) 14 days after sampler insertion and (B) 21 days after sampler insertion (right panel). Error bars depict one standard deviation. Passive sampler MeHg concentrations rose significantly in both water and sediment between days 14 and 21 of exposure. There were no significant differences in MeHg uptake between sheet and split samplers deployed within each matrix (sediment vs. water). Analysis based on standard least squares models that considered time, sampler type, and sampler placement with an overall =0.05.

Figure S9

Comparison of log(K) values for partitioning of MeHg from porewater to either sediment (solid bars) or passive samplers inserted within the sediment phase (dashed bars) in sediment microcosms at 14 days and 21 days after passive sampler deployment. Bars show average 1 standard deviation for triplicate microcosms at each time point. Colored bars represent three treatments: no passive sampler (green), sheet-ps (blue) or split-ps (orange).

Figure S10

Calculated MeHg speciation in microcosm surface waters and porewaters as a function of the DOM thiol concentration (DOM-RS) and the sum of low molecular weight thiols. Calculations were performed using minimum and maximum estimated values of the formation constants (Kf) for MeHg complexes with low molecular weight thiols and DOM thiols, see Table S9 for equations and references. For surface water models (A &B), pH = 7.7, Cl- = 5×10-2 M, and sulfide = 0 M,, while for porewater models (C& D), , pH = 6.8, Cl- = 6.5×10-2 M, and sulfide = 2×10-6 M, average measured conditions for the microcosms. A) Formation constants most favoring MeHg(LMM-RS) complexes in surface water; B) formation constants most favoring MeHg(DOM-RS) complexes in porewater, C) formation constants most favoring MeHgSH over MeHg(LMM-RS) and MeHg(DOM-RS) complexes in porewater; D) formation constants most favoring MeHg(LMM-RS) and MeHg(DOM-RS) complexes over MeHgSH in porewater. Orange boxes show the estimated range of LMM-RS and DOM-RS in microcosm surface water or porewater (see text).

- log Kf MeHg(LMM-RS) = 15.7 log Kf MeHg(DOM-RS)= 17.1

- log Kf MeHg(LMM-RS) = 17.5 log Kf MeHg(DOM-RS)= 15.6

- log Kf MeHg(LMM-RS) = 15.7 log Kf MeHg(DOM-RS)= 15.6

- log Kf MeHg(LMM-RS) = 17.5 log Kf MeHg(DOM-RS)= 17.1

Supplemental Tables

Table S1

Reference Organic Matter stock elemental composition and C distributions. All data are taken from IHSS.

| OM Source | Abbreviation | C content (mass %) | S content (mass %) | S/C | Aromaticity (% of C) |
| --- | --- | --- | --- | --- | --- |
| Suwannee River Humic Acid III | SRHA | 54.59 | 0.55 | 0.010 | 35.3 |
| Suwannee River Fulvic Acid II | SRFA | 52.34 | 0.46 | 0.009 | 22 |
| Elliott Soil Humic Acid V | ESHA | 58.75 | 0.43 | 0.007 | 48.3 |
| Pahokee Peat Humic Acid II | PPHA | 56.37 | 0.71 | 0.013 | 47 |
| Leonardite Humic Acid | LHA | 63.81 | 0.76 | 0.012 | 58 |
| Suwannee River Natural Organic Matter | SRNOM | 50.7 | 1.78 | 0.035 | 23 |
| Upper Mississippi River Natural Organic Matter | UMRNOM | 49.98 | 2.62 | 0.052 | 19 |

Table S2

Quality assurance data for MeHg analyses in this work.a

| Matrix | RPD Duplicates | Concentration | ID Spike Recovery | CRM Recovery | DL | Units |
| --- | --- | --- | --- | --- | --- | --- |
| water | 5.4 ± 5.0% | NA | 83.3 ± 12.9% | NA | 0.48 ± 0.74 | ng L-1 |
| sediment | 15.7% | NA | 82.1 ± 21.5% | NA | 2057 ± 673 | ng kgdw-1 |
| ag+AC | n/a | NA | 65.8 ± 12.5% | NA | 83.7 ± 207 | ng kgdw-1 |
| bare AC particles | n/a | NA | 47.6% ± 9.7% | NA | 0.36 ± 0.35 | ng kgdw-1 |
| CRM | NA | 13.06 ± 1.59 | 87.5% ± 9.7% | 95.3% ±10.3% | NA | g gdw-1 |
| distillation blanks | NA | 0.11 ± 0.10 | 72.2% ± 12.2% | NA | NA | ng L-1 |

a Analysis was done by isotope dilution ICP-MS, i.e., with internal stable isotope standards. Relative percent differences (RPD) are for duplicate analyses of the same prepared sample. Certified Reference Materials (CRM) were NIST 1566b oyster tissue, certified concentration of 13.2 g/g MeHg. Detection limits were estimated as three times the standard error of blanks across samples.

Table S3

Summary of MeHgCys isotherm experiment data.

| MeHg Spike Level (ng/L) | Replicate | Sample Type | Sorbent | Mass (g) | MeHg Conc. (ng/L or ng/kg) | Treatment Avg. MeHg Conc. (ng/L or ng/kg) | 1 SD of MeHg Conc. | Log(Cw) | Log(Cps) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DI Blank | A | Water | Blank | 40 | 0.21 |  |  |  |  |
| DI Blank | B | Water | Blank | 40 | 0.21 | 0.20 | 0.03 |  |  |
| DI Blank | C | Water | Blank | 40 | 0.17 |  |  |  |  |
| Control Blank | A | Water | Blank | 40 | 0.14 |  |  |  |  |
| Control Blank | B | Water | Blank | 40 | 0.16 | 0.14 | 0.02 |  |  |
| Control Blank | C | Water | Blank | 40 | 0.12 |  |  |  |  |
| Control Blank | A | Water | AC | 30 | 0.16 |  |  |  |  |
| Control Blank | B | Water | AC | 30 | 0.16 | 0.16 | 0.00 |  |  |
| Control Blank | C | Water | AC | 30 | 0.16 |  |  |  |  |
| Control Blank | A | Particles | AC | 0.0098 | 299 |  |  |  |  |
| Control Blank | B | Particles | AC | 0.0094 | 314 | 282.31 | 43.06 |  |  |
| Control Blank | C | Particles | AC | 0.0101 | 233 |  |  |  |  |
| 3 | A | Water | AC | 30 | 0.25 |  |  |  |  |
| 3 | B | Water | AC | 30 | 0.21 | 0.21 | 0.04 | -0.68 |  |
| 3 | C | Water | AC | 30 | 0.17 |  |  |  |  |
| 3 | A | Particles | AC | 0.0093 | 11132 |  |  |  |  |
| 3 | B | Particles | AC | 0.0094 | 9797 | 10580.62 | 696.84 |  | 4.02 |
| 3 | C | Particles | AC | 0.0098 | 10812 |  |  |  |  |
| 10 | A | Water | AC | 30 | 0.59 |  |  |  |  |
| 10 | B | Water | AC | 30 | 0.51 | 0.57 | 0.05 | -0.24 |  |
| 10 | C | Water | AC | 30 | 0.61 |  |  |  |  |
| 10 | A | Particles | AC | 0.0104 | 26920 |  |  |  |  |
| 10 | B | Particles | AC | 0.0113 | 24398 | 27990.92 | 4231.42 |  | 4.45 |
| 10 | C | Particles | AC | 0.0092 | 32655 |  |  |  |  |
| 30 | A | Water | AC | 30 | 1.48 |  |  |  |  |
| 30 | B | Water | AC | 30 | 1.49 | 1.49 | 0.01 | 0.17 |  |
| 30 | C | Water | AC | 30 |  |  |  |  |  |
| 30 | A | Particles | AC | 0.0117 | 64533 |  |  |  |  |
| 30 | B | Particles | AC | 0.0099 | 73860 | 69525.97 | 4698.11 |  | 4.84 |
| 30 | C | Particles | AC | 0.0105 | 70185 |  |  |  |  |
| 100 | A | Water | AC | 30 | 2.39 |  |  |  |  |
| 100 | B | Water | AC | 30 | 2.80 | 2.75 | 0.34 | 0.44 |  |
| 100 | C | Water | AC | 30 | 3.06 |  |  |  |  |
| 100 | A | Particles | AC | 0.0109 | 253118 |  |  |  |  |
| 100 | B | Particles | AC | 0.0108 | 253231 | 255437.07 | 3919.14 |  | 5.41 |
| 100 | C | Particles | AC | 0.0104 | 259962 |  |  |  |  |
| 300 | A | Water | AC | 30 | 7.04 |  |  |  |  |
| 300 | B | Water | AC | 30 | 6.63 | 6.94 | 0.28 | 0.84 |  |
| 300 | C | Water | AC | 30 | 7.16 |  |  |  |  |
| 300 | A | Particles | AC | 0.0117 | 652425 |  |  |  |  |
| 300 | B | Particles | AC | 0.011 | 720921 | 793755.64 | 188608.05 |  | 5.90 |
| 300 | C | Particles | AC | 0.0105 | 1007921 |  |  |  |  |
| Control Blank | A | Water | ag+AC | 30 | 0.13 |  |  |  |  |
| Control Blank | B | Water | ag+AC | 30 | 0.15 | 0.13 | 0.01 | -0.87 |  |
| Control Blank | C | Water | ag+AC | 30 | 0.13 |  |  |  |  |
| Control Blank | A | Sampler | ag+AC | 0.446 | 5 |  |  |  |  |
| Control Blank | B | Sampler | ag+AC | 0.43 | 5 | 5.64 | 0.58 |  |  |
| Control Blank | C | Sampler | ag+AC | 0.45 | 6 |  |  |  |  |
| 30 | A | Water | ag+AC | 30 | 1.44 |  |  |  |  |
| 30 | B | Water | ag+AC | 30 | 1.45 | 1.45 | 0.02 | 0.16 |  |
| 30 | C | Water | ag+AC | 30 | 1.47 |  |  |  |  |
| 30 | A | Sampler | ag+AC | 0.468 | 1952 |  |  |  |  |
| 30 | B | Sampler | ag+AC | 0.478 | 1826 | 1821.37 | 132.92 |  | 3.26 |
| 30 | C | Sampler | ag+AC | 0.491 | 1686 |  |  |  |  |
| 100 | A | Water | ag+AC | 30 | 2.67 |  |  |  |  |
| 100 | B | Water | ag+AC | 30 | 2.79 | 2.71 | 0.07 | 0.43 |  |
| 100 | C | Water | ag+AC | 30 | 2.66 |  |  |  |  |
| 100 | A | Sampler | ag+AC | 0.445 | 6612 |  |  |  |  |
| 100 | B | Sampler | ag+AC | 0.405 | 7190 | 6596.39 | 601.51 |  | 3.82 |
| 100 | C | Sampler | ag+AC | 0.481 | 5987 |  |  |  |  |
| 300 | A | Water | ag+AC | 30 | 10.52 |  |  |  |  |
| 300 | B | Water | ag+AC | 30 | 11.44 | 11.41 | 0.89 | 1.06 |  |
| 300 | C | Water | ag+AC | 30 | 12.29 |  |  |  |  |
| 300 | A | Sampler | ag+AC | 0.481 | 18942 |  |  |  |  |
| 300 | B | Sampler | ag+AC | 0.459 | 18087 | 18628.48 | 471.19 |  | 4.27 |
| 300 | C | Sampler | ag+AC | 0.463 | 18857 |  |  |  |  |
| 1000 | A | Water | ag+AC | 30 | 36.80 |  |  |  |  |
| 1000 | B | Water | ag+AC | 30 | 32.43 | 32.05 | 4.94 | 1.51 |  |
| 1000 | C | Water | ag+AC | 30 | 26.93 |  |  |  |  |
| 1000 | A | Sampler | ag+AC | 0.471 | 59993 |  |  |  |  |
| 1000 | B | Sampler | ag+AC | 0.594 | 48463 | 55398.41 | 6111.18 |  | 4.74 |
| 1000 | C | Sampler | ag+AC | 0.465 | 57740 |  |  |  |  |
| 3000 | A | Water | ag+AC | 30 | 173.54 |  |  |  |  |
| 3000 | B | Water | ag+AC | 30 | 141.20 | 153.09 | 17.79 | 2.18 |  |
| 3000 | C | Water | ag+AC | 30 | 144.53 |  |  |  |  |
| 3000 | A | Sampler | ag+AC | 0.43 | 180870 |  |  |  |  |
| 3000 | B | Sampler | ag+AC | 0.543 | 130424 | 159927.52 | 26290.22 |  | 5.20 |
| 3000 | C | Sampler | ag+AC | 0.475 | 168488 |  |  |  |  |

Table S4

Summary of experimental data from MeHgDOM isotherm experiments. DOM source abbreviations are taken from Table S1.

| Isotherm Experiment | Adsorbate | Sample Type | DOM Source | Mass of Reservoir (g) | MeHg (ng/L or ng/kg) | DOC (mg/L) |
| --- | --- | --- | --- | --- | --- | --- |
| Varying DOM:MeHg | Blank | Water | SRFA | 35 | 0.13 | 1.09 |
| Varying DOM:MeHg | MeHg | Water | SRFA | 35 | 0.59 | 4.15 |
| Varying DOM:MeHg | MeHg | Water | SRFA | 35 | 2.69 | 1.22 |
| Varying DOM:MeHg | MeHg | Water | SRFA | 35 | 5.22 | 1.35 |
| Varying DOM:MeHg | MeHg | Water | SRFA | 35 | 23.76 | 1.63 |
| Varying DOM:MeHg | Blank | Polymer | SRFA | 0.85 | 8.34 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRFA | 0.718 | 232.19 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRFA | 0.748 | 1199.58 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRFA | 0.736 | 2480.47 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRFA | 0.667 | 11680.83 |  |
| Varying DOM:MeHg | Blank | Water | SRNOM | 35 | 0.08 | 1.07 |
| Varying DOM:MeHg | MeHg | Water | SRNOM | 35 | 0.42 | 4.01 |
| Varying DOM:MeHg | MeHg | Water | SRNOM | 35 | 2.19 | 1.20 |
| Varying DOM:MeHg | MeHg | Water | SRNOM | 35 | 6.23 | 1.16 |
| Varying DOM:MeHg | MeHg | Water | SRNOM | 35 | 18.30 | 1.03 |
| Varying DOM:MeHg | Blank | Polymer | SRNOM | 0.809 | 5.57 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRNOM | 0.728 | 196.39 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRNOM | 0.767 | 1109.07 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRNOM | 0.8 | 2097.87 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRNOM | 0.813 | 10375.62 |  |
| Varying DOM:MeHg | Blank | Water | UMRNOM | 35 | 0.01 | 1.10 |
| Varying DOM:MeHg | MeHg | Water | UMRNOM | 35 | 0.25 | 4.11 |
| Varying DOM:MeHg | MeHg | Water | UMRNOM | 35 | 1.46 | 1.29 |
| Varying DOM:MeHg | MeHg | Water | UMRNOM | 35 | 3.18 | 1.23 |
| Varying DOM:MeHg | MeHg | Water | UMRNOM | 35 | 7.02 | 1.37 |
| Varying DOM:MeHg | Blank | Polymer | UMRNOM | 0.815 | 7.29 |  |
| Varying DOM:MeHg | MeHg | Polymer | UMRNOM | 0.851 | 193.55 |  |
| Varying DOM:MeHg | MeHg | Polymer | UMRNOM | 0.836 | 1065.83 |  |
| Varying DOM:MeHg | MeHg | Polymer | UMRNOM | 0.803 | 2167.44 |  |
| Varying DOM:MeHg | MeHg | Polymer | UMRNOM | 0.819 | 9567.57 |  |
| Varying DOM:MeHg | Blank | Water | ESHA | 35 | 0.00 | 2.48 |
| Varying DOM:MeHg | MeHg | Water | ESHA | 35 | 0.94 | 5.73 |
| Varying DOM:MeHg | MeHg | Water | ESHA | 35 | 4.73 | 3.02 |
| Varying DOM:MeHg | MeHg | Water | ESHA | 35 | 7.52 | 2.18 |
| Varying DOM:MeHg | MeHg | Water | ESHA | 35 | 37.75 | 2.65 |
| Varying DOM:MeHg | Blank | Polymer | ESHA | 0.809 | 0.23 |  |
| Varying DOM:MeHg | MeHg | Polymer | ESHA | 0.835 | 185.83 |  |
| Varying DOM:MeHg | MeHg | Polymer | ESHA | 0.766 | 1124.06 |  |
| Varying DOM:MeHg | MeHg | Polymer | ESHA | 0.819 | 2183.05 |  |
| Varying DOM:MeHg | MeHg | Polymer | ESHA | 0.768 | 14541.28 |  |
| Varying DOM:MeHg | Blank | Water | PPHA | 35 | 0.00 | 1.94 |
| Varying DOM:MeHg | MeHg | Water | PPHA | 35 | 1.78 | 4.55 |
| Varying DOM:MeHg | MeHg | Water | PPHA | 35 | 8.33 | 1.93 |
| Varying DOM:MeHg | MeHg | Water | PPHA | 35 | 15.49 | 2.04 |
| Varying DOM:MeHg | MeHg | Water | PPHA | 35 | 64.44 | 2.48 |
| Varying DOM:MeHg | Blank | Polymer | PPHA | 0.8 | 1.85 |  |
| Varying DOM:MeHg | MeHg | Polymer | PPHA | 0.842 | 162.45 |  |
| Varying DOM:MeHg | MeHg | Polymer | PPHA | 0.819 | 887.05 |  |
| Varying DOM:MeHg | MeHg | Polymer | PPHA | 0.783 | 2018.64 |  |
| Varying DOM:MeHg | MeHg | Polymer | PPHA | 0.803 | 11933.00 |  |
| Varying DOM:MeHg | Blank | Water | LHA | 35 | 0.00 | 1.26 |
| Varying DOM:MeHg | MeHg | Water | LHA | 35 | 1.51 | 4.54 |
| Varying DOM:MeHg | MeHg | Water | LHA | 35 | 5.71 | 1.50 |
| Varying DOM:MeHg | MeHg | Water | LHA | 35 | 10.11 | 1.59 |
| Varying DOM:MeHg | MeHg | Water | LHA | 35 | 36.35 | 2.22 |
| Varying DOM:MeHg | Blank | Polymer | LHA | 0.921 | 0.00 |  |
| Varying DOM:MeHg | MeHg | Polymer | LHA | 0.805 | 163.50 |  |
| Varying DOM:MeHg | MeHg | Polymer | LHA | 0.904 | 936.34 |  |
| Varying DOM:MeHg | MeHg | Polymer | LHA | 0.838 | 1739.44 |  |
| Varying DOM:MeHg | MeHg | Polymer | LHA | 1.039 | 10213.95 |  |
| Varying DOM:MeHg | Blank | Water | SRHA | 35 | 0.00 | 2.86 |
| Varying DOM:MeHg | MeHg | Water | SRHA | 35 | 1.95 | 6.10 |
| Varying DOM:MeHg | MeHg | Water | SRHA | 35 | 8.92 | 3.11 |
| Varying DOM:MeHg | MeHg | Water | SRHA | 35 | 19.95 | 2.91 |
| Varying DOM:MeHg | MeHg | Water | SRHA | 35 | 99.78 | 3.67 |
| Varying DOM:MeHg | Blank | Polymer | SRHA | 0.779 | 0.93 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRHA | 0.877 | 134.14 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRHA | 0.871 | 612.39 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRHA | 0.848 | 1690.84 |  |
| Varying DOM:MeHg | MeHg | Polymer | SRHA | 0.838 | 9300.67 |  |
| Constant DOM:MeHg | MeHg | Water | ESHA | 30 | 1.50 |  |
| Constant DOM:MeHg | MeHg | Water | ESHA | 30 | 7.20 |  |
| Constant DOM:MeHg | MeHg | Water | ESHA | 30 | 12.85 |  |
| Constant DOM:MeHg | MeHg | Polymer | ESHA | 0.732 | 318.21 |  |
| Constant DOM:MeHg | MeHg | Polymer | ESHA | 0.61 | 943.69 |  |
| Constant DOM:MeHg | MeHg | Polymer | ESHA | 0.466 | 1864.54 |  |
| Constant DOM:MeHg | MeHg | Water | LHA | 30 | 2.28 |  |
| Constant DOM:MeHg | MeHg | Water | LHA | 30 | 8.65 |  |
| Constant DOM:MeHg | MeHg | Water | LHA | 30 | 13.86 |  |
| Constant DOM:MeHg | MeHg | Polymer | LHA | 0.862 | 267.22 |  |
| Constant DOM:MeHg | MeHg | Polymer | LHA | 0.899 | 574.11 |  |
| Constant DOM:MeHg | MeHg | Polymer | LHA | 0.823 | 860.72 |  |
| Constant DOM:MeHg | MeHg | Water | PPHA | 30 | 0.80 |  |
| Constant DOM:MeHg | MeHg | Water | PPHA | 30 | 5.49 |  |
| Constant DOM:MeHg | MeHg | Water | PPHA | 30 | 11.06 |  |
| Constant DOM:MeHg | MeHg | Polymer | PPHA | 0.755 | 353.41 |  |
| Constant DOM:MeHg | MeHg | Polymer | PPHA | 0.741 | 1156.81 |  |
| Constant DOM:MeHg | MeHg | Polymer | PPHA | 0.77 | 1203.97 |  |
| Constant DOM:MeHg | MeHg | Water | SRFA | 30 | 0.09 |  |
| Constant DOM:MeHg | MeHg | Water | SRFA | 30 | 1.38 |  |
| Constant DOM:MeHg | MeHg | Water | SRFA | 30 | 8.00 |  |
| Constant DOM:MeHg | MeHg | Water | SRFA | 30 | 59.82 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRFA | 0.827 | 8.15 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRFA | 0.731 | 332.24 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRFA | 0.845 | 477.15 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRFA | 0.816 | 956.89 |  |
| Constant DOM:MeHg | MeHg | Water | SRNOM | 30 | 0.06 |  |
| Constant DOM:MeHg | MeHg | Water | SRNOM | 30 | 0.09 |  |
| Constant DOM:MeHg | MeHg | Water | SRNOM | 30 | 0.70 |  |
| Constant DOM:MeHg | MeHg | Water | SRNOM | 30 | 6.41 |  |
| Constant DOM:MeHg | MeHg | Water | SRNOM | 30 | 46.29 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRNOM | 0.749 | 9.29 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRNOM | 0.694 | 40.60 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRNOM | 0.758 | 337.34 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRNOM | 0.807 | 560.59 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRNOM | 0.999 | 944.41 |  |
| Constant DOM:MeHg | MeHg | Water | UMRNOM | 30 | 0.13 |  |
| Constant DOM:MeHg | MeHg | Water | UMRNOM | 30 | 0.04 |  |
| Constant DOM:MeHg | MeHg | Water | UMRNOM | 30 | 0.70 |  |
| Constant DOM:MeHg | MeHg | Water | UMRNOM | 30 | 5.90 |  |
| Constant DOM:MeHg | MeHg | Water | UMRNOM | 30 | 41.30 |  |
| Constant DOM:MeHg | MeHg | Polymer | UMRNOM | 0.829 | 8.51 |  |
| Constant DOM:MeHg | MeHg | Polymer | UMRNOM | 0.873 | 32.95 |  |
| Constant DOM:MeHg | MeHg | Polymer | UMRNOM | 0.844 | 308.96 |  |
| Constant DOM:MeHg | MeHg | Polymer | UMRNOM | 0.795 | 611.45 |  |
| Constant DOM:MeHg | MeHg | Polymer | UMRNOM | 0.868 | 1451.39 |  |
| Constant DOM:MeHg | MeHg | Water | SRHA | 30 | 0.96 |  |
| Constant DOM:MeHg | MeHg | Water | SRHA | 30 | 3.02 |  |
| Constant DOM:MeHg | MeHg | Water | SRHA | 30 | 20.98 |  |
| Constant DOM:MeHg | MeHg | Water | SRHA | 30 | 26.98 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRHA | 0.73 | 221.52 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRHA | 0.793 | 352.45 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRHA | 0.639 | 1479.10 |  |
| Constant DOM:MeHg | MeHg | Polymer | SRHA | 0.736 | 954.55 |  |

Table S5

Summary of isotopically labelled MeHgSRHA:MeHgSRHA exchange experiment data. Samples are broken down by whether they were a part of the uptake or exchange phase, whether the MeHg concentrations were measured in overlying water or sorbent material, and by sorbent. Control samples contained MeXXXHgSRHA spikes, but no sorbent materials. Averages and standard deviation of MeXXXHg concentrations are shown for triplicate treatments at each timepoint.

| Phase | Sample Type | Sorbent | Replicate | Time (min) | Mass of Reservoir (g) | Me199Hg (ng/L or ng/kg) | Treatment Avg. Me199Hg | 1 SD | Log(Kps) Me199Hg | Me198Hg (ng/L or ng/kg) | Treatment Avg. Me198Hg | 1 SD | Log(Kps) Me198Hg | Overall Log(Kps) | DOC (mg C/L) | Treatment Avg. DOC | 1SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Uptake | Water | Blank | A | 21500 | 30 | 0.00 |  |  |  | 0.00 |  |  |  |  |  |  |  |
| Uptake | Water | Blank | B | 21500 | 30 | 0.00 | 0.00 | 0.00 |  | 0.00 | 0.00 | 0.00 |  |  |  |  |  |
| Uptake | Water | Blank | C | 21500 | 30 | 0.00 |  |  |  | 0.00 |  |  |  |  |  |  |  |
| Uptake | Water | Control | A | 0 | 30 | 50.81 |  |  |  | 0.00 |  |  |  |  |  |  |  |
| Uptake | Water | Control | B | 0 | 30 | 46.07 | 49.52 | 3.03 |  | 0.00 | 0.01 | 0.01 |  |  |  |  |  |
| Uptake | Water | Control | A | 0 | 30 | 51.70 |  |  |  | 0.02 |  |  |  |  |  |  |  |
| Uptake | Water | Control | A | 2850 | 30 | 47.44 |  |  |  | 0.00 |  |  |  |  | 5.41 |  |  |
| Uptake | Water | Control | B | 2850 | 30 | 50.92 | 50.43 | 2.78 |  | 0.00 | 0.00 | 0.00 |  |  | 5.85 | 5.92 | 0.56 |
| Uptake | Water | Control | C | 2850 | 30 | 52.94 |  |  |  | 0.00 |  |  |  |  | 6.51 |  |  |
| Uptake | Water | Control | A | 21500 | 30 | 54.71 |  |  |  | 0.00 |  |  |  |  | 5.65 |  |  |
| Uptake | Water | Control | B | 21500 | 30 | 55.06 | 53.78 | 1.92 |  | 0.00 | 0.00 | 0.00 |  |  | 5.67 | 5.53 | 0.24 |
| Uptake | Water | Control | C | 21500 | 30 | 51.57 |  |  |  | 0.00 |  |  |  |  | 5.255 |  |  |
| Uptake | Sorbent | ag+AC Sampler | A | 21500 | 0.84 | 593.85 |  |  |  | 3.22 |  |  |  |  |  |  |  |
| Uptake | Sorbent | ag+AC Sampler | B | 21500 | 0.90 | 515.27 | 554.56 | 55.56 |  | 3.79 | 3.51 | 0.40 |  |  |  |  |  |
| Uptake | Water | ag+AC Sampler | A | 21500 | 30 | 31.20 |  |  |  | 0.00 |  |  |  |  | 4.68 |  |  |
| Uptake | Water | ag+AC Sampler | B | 21500 | 30 | 30.67 | 30.94 | 0.38 | 1.194 | 0.00 | 0.00 | 0.00 | NA | 1.194 | 3.84 | 4.26 | 0.59 |
| Uptake | Water | ag+AC Sampler | A | 21500 | 30 | 35.48 |  |  |  | 0.00 |  |  |  |  | 3.96 |  |  |
| Uptake | Water | ag+AC Sampler | B | 21500 | 30 | 34.89 |  |  |  | 0.00 |  |  |  |  | 4.54 |  |  |
| Uptake | Water | ag+AC Sampler | C | 21500 | 30 | 38.25 |  |  |  | 0.00 |  |  |  |  | 4.37 |  |  |
| Uptake | Water | ag+AC Sampler | D | 21500 | 30 | 36.64 |  |  |  | 0.00 |  |  |  |  | 5.49 |  |  |
| Uptake | Water | ag+AC Sampler | E | 21500 | 30 | 35.13 |  |  |  | 0.00 |  |  |  |  | 4.29 |  |  |
| Uptake | Water | ag+AC Sampler | F | 21500 | 30 | 36.71 | 36.22 | 1.37 |  | 0.00 | 0.00 | 0.00 |  |  | 4.256 | 4.27 | 0.48 |
| Uptake | Water | ag+AC Sampler | G | 21500 | 30 | 36.52 |  |  |  | 0.00 |  |  |  |  | 4.151 |  |  |
| Uptake | Water | ag+AC Sampler | H | 21500 | 30 | 36.50 |  |  |  | 0.00 |  |  |  |  | 3.923 |  |  |
| Uptake | Water | ag+AC Sampler | I | 21500 | 30 | 38.71 |  |  |  | 0.00 |  |  |  |  | 3.569 |  |  |
| Uptake | Water | ag+AC Sampler | J | 21500 | 30 | 36.52 |  |  |  | 0.00 |  |  |  |  | 3.87 |  |  |
| Uptake | Water | ag+AC Sampler | K | 21500 | 30 | 35.46 |  |  |  | 0.00 |  |  |  |  | 4.29 |  |  |
| Uptake | Water | ag+AC Sampler | L | 21500 | 30 | 33.85 |  |  |  | 0.00 |  |  |  |  | 4.52 |  |  |
| Uptake | Sorbent | Bare AC Particle | A | 2850 | 0.0111 | 35913.44 |  |  |  | 653.61 |  |  |  |  |  |  |  |
| Uptake | Sorbent | Bare AC Particle | B | 2850 | 0.0112 | 35836.77 | 35875.10 | 54.22 |  | 0.00 | 326.80 | 462.17 |  |  |  |  |  |
| Uptake | Water | Bare AC Particle | A | 2850 | 30 | 36.85 |  |  |  | 0.24 |  |  |  |  | 6.66 |  |  |
| Uptake | Water | Bare AC Particle | B | 2850 | 30 | 34.02 | 35.43 | 2.00 | 2.98 | 0.00 | 0.12 | 0.17 | NA | 2.98 | 5.89 | 6.27 | 0.55 |
| Uptake | Water | Bare AC Particle | A | 2850 | 30 | 33.54 |  |  |  | 0.19 |  |  |  |  | 4.74 |  |  |
| Uptake | Water | Bare AC Particle | B | 2850 | 30 | 33.34 |  |  |  | 0.00 |  |  |  |  | 3.84 |  |  |
| Uptake | Water | Bare AC Particle | C | 2850 | 30 | 35.49 |  |  |  | 0.00 |  |  |  |  | 4.011 |  |  |
| Uptake | Water | Bare AC Particle | D | 2850 | 30 | 31.84 |  |  |  | 0.00 |  |  |  |  | 4.65 |  |  |
| Uptake | Water | Bare AC Particle | E | 2850 | 30 | 31.69 | 31.75 | 4.27 |  | 0.00 | 0.02 | 0.06 |  |  | 4.35 | 4.56 | 0.49 |
| Uptake | Water | Bare AC Particle | I | 2850 | 30 | 27.29 |  |  |  | 0.00 |  |  |  |  | 4.039 |  |  |
| Uptake | Water | Bare AC Particle | J | 2850 | 30 | 37.28 |  |  |  | 0.00 |  |  |  |  | 5.475 |  |  |
| Uptake | Water | Bare AC Particle | K | 2850 | 30 | 32.24 |  |  |  | 0.00 |  |  |  |  | 5.19 |  |  |
| Uptake | Water | Bare AC Particle | L | 2850 | 30 | 23.05 |  |  |  | 0.00 |  |  |  |  | 4.86 |  |  |
| Uptake | Water | Bare AC Particle | F | 2850 | 30 | NA |  |  |  | NA |  |  |  |  | 4.28 |  |  |
| Uptake | Water | Bare AC Particle | G | 2850 | 30 | NA |  |  |  | NA |  |  |  |  | 4.78 |  |  |
| Uptake | Water | Bare AC Particle | H | 2850 | 30 | NA |  |  |  | NA |  |  |  |  | 4.472 |  |  |
| Exchange | Water | Blank | A | 20194 | 30 | 0.00 |  |  |  | 0.00 |  |  |  |  | 0.67 |  |  |
| Exchange | Water | Blank | B | 20194 | 30 | 0.00 | 0.00 | 0.00 |  | 0.00 | 0.00 | 0.00 |  |  | 0.557 | 0.57 | 0.08 |
| Exchange | Water | Blank | C | 20194 | 30 | 0.00 |  |  |  | 0.00 |  |  |  |  | 0.50 |  |  |
| Exchange | Water | Control | A | 0 | 30 | 0.43 |  |  |  | 41.44 |  |  |  |  |  |  |  |
| Exchange | Water | Control | B | 0 | 30 | 0.45 | 0.44 | 0.01 |  | 44.93 | 43.19 | 2.47 |  |  |  |  |  |
| Exchange | Water | Control | A | 0 | 30 | 0.34 |  |  |  | 42.30 |  |  |  |  | 7.23 |  |  |
| Exchange | Water | Control | B | 0 | 30 | 0.39 | 0.37 | 0.03 |  | 41.63 | 41.96 | 0.48 |  |  | 7.22 | 7.23 | 0.01 |
| Exchange | Water | Control | A | 187 | 30 | 1.97 |  |  |  | 39.43 |  |  |  |  |  |  |  |
| Exchange | Water | Control | B | 187 | 30 | 0.54 | 1.37 | 0.74 |  | 43.91 | 42.00 | 2.31 |  |  |  |  |  |
| Exchange | Water | Control | C | 187 | 30 | 1.61 |  |  |  | 42.66 |  |  |  |  |  |  |  |
| Exchange | Water | Control | A | 2875 | 30 | 0.26 |  |  |  | 40.89 |  |  |  |  | 5.20 |  |  |
| Exchange | Water | Control | B | 2875 | 30 | 0.00 | 0.19 | 0.17 |  | 44.07 | 42.17 | 1.68 |  |  | 5.22 | 5.15 | 0.10 |
| Exchange | Water | Control | C | 2875 | 30 | 0.31 |  |  |  | 41.54 |  |  |  |  | 5.026 |  |  |
| Exchange | Water | Control | A | 10094 | 30 | 0.09 |  |  |  | 34.97 |  |  |  |  |  |  |  |
| Exchange | Water | Control | B | 10094 | 30 | 0.04 | 0.04 | 0.04 |  | 38.19 | 37.60 | 2.38 |  |  |  |  |  |
| Exchange | Water | Control | C | 10094 | 30 | 0.00 |  |  |  | 39.63 |  |  |  |  |  |  |  |
| Exchange | Water | Control | A | 20194 | 30 | 0.00 |  |  |  | 33.55 |  |  |  |  | 6.524 |  |  |
| Exchange | Water | Control | B | 20194 | 30 | 0.00 | 0.00 | 0.00 |  | 34.63 | 34.84 | 1.40 |  |  | 7.030 | 6.94 | 0.38 |
| Exchange | Water | Control | C | 20194 | 30 | 0.00 |  |  |  | 36.33 |  |  |  |  | 7.273 |  |  |
| Exchange | Sorbent | ag+AC Sampler | A | 81 | 0.83 | 522.00 |  |  |  | 64.90 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | B | 81 | 0.77 | 677.96 | 599.98 | 110.28 |  | 26.49 | 45.69 | 27.16 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | A | 81 | 30 | 0.89 |  |  |  | 34.84 |  |  |  |  | 6.72 |  |  |
| Exchange | Water | ag+AC Sampler | B | 81 | 30 | 1.87 | 1.38 | 0.70 | 2.638 | 32.54 | 33.69 | 1.62 | 0.132 | 1.265 | 6.639 | 6.68 | 0.06 |
| Exchange | Sorbent | ag+AC Sampler | A | 369 | 0.74 | 595.65 |  |  |  | 55.97 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | B | 369 | 0.70 | 601.15 | 598.40 | 3.89 |  | 68.05 | 62.01 | 8.54 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | A | 369 | 30 | 1.75 |  |  |  | 35.60 |  |  |  |  | 7.14 |  |  |
| Exchange | Water | ag+AC Sampler | B | 369 | 30 | 0.66 | 1.20 | 0.77 | 2.696 | 34.49 | 35.04 | 0.79 | 0.248 | 1.261 | 6.94 | 7.04 | 0.14 |
| Exchange | Sorbent | ag+AC Sampler | B | 1556 | 0.74 | 554.04 |  |  |  | 102.64 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | A | 1556 | 0.75 | 560.14 | 557.09 | 4.32 |  | 108.42 | 105.53 | 4.09 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | B | 1556 | 30 | 1.71 |  |  |  | 30.40 |  |  |  |  | 7.65 |  |  |
| Exchange | Water | ag+AC Sampler | A | 1556 | 30 | 1.25 | 1.48 | 0.32 | 2.575 | 33.30 | 31.85 | 2.05 | 0.520 | 1.298 | 7.39 | 7.52 | 0.18 |
| Exchange | Sorbent | ag+AC Sampler | A | 3111 | 0.76 | 512.73 |  |  |  | 123.45 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | B | 3111 | 0.71 | 559.19 | 535.96 | 32.85 |  | 154.64 | 139.04 | 22.06 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | A | 3111 | 30 | 2.04 |  |  |  | 31.87 |  |  |  |  | 7.491 |  |  |
| Exchange | Water | ag+AC Sampler | B | 3111 | 30 | 2.04 | 2.04 | 0.00 | 2.420 | 31.67 | 31.77 | 0.15 | 0.641 | 1.300 | 7.503 | 7.50 | 0.01 |
| Exchange | Sorbent | ag+AC Sampler | A | 10094 | 0.71 | 452.67 |  |  |  | 204.77 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | B | 10094 | 0.71 | 385.72 | 419.19 | 47.34 |  | 191.04 | 197.90 | 9.71 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | A | 10094 | 30 | 3.98 |  |  |  | 30.45 |  |  |  |  | 6.09 |  |  |
| Exchange | Water | ag+AC Sampler | B | 10094 | 30 | 4.04 | 4.01 | 0.04 | 2.020 | 32.73 | 31.59 | 1.62 | 0.797 | 1.239 | 6.572 | 6.33 | 0.34 |
| Exchange | Sorbent | ag+AC Sampler | A | 20194 | 0.78 | 383.71 |  |  |  | 250.09 |  |  |  |  |  |  |  |
| Exchange | Sorbent | ag+AC Sampler | B | 20194 | 0.69 | 326.43 | 355.07 | 40.51 |  | 268.93 | 259.51 | 13.32 |  |  |  |  |  |
| Exchange | Water | ag+AC Sampler | A | 20194 | 30 | 5.10 |  |  |  | 29.05 |  |  |  |  | 6.15 |  |  |
| Exchange | Water | ag+AC Sampler | B | 20194 | 30 | 4.68 | 4.89 | 0.30 | 1.861 | 28.74 | 28.89 | 0.22 | 0.953 | 1.260 | 6.57 | 6.36 | 0.30 |
| Exchange | Sorbent | Bare AC Particle | A | 21 | 0.0106 | 24741.86 |  |  |  | 4322.80 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | B | 21 | 0.0116 | 26219.36 | 25480.61 | 1044.75 |  | 4392.47 | 4357.63 | 49.26 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | A | 21 | 30 | 1.60 |  |  |  | 37.21 |  |  |  |  | 5.64 |  |  |
| Exchange | Water | Bare AC Particle | B | 21 | 30 | 1.21 | 1.41 | 0.28 | 4.26 | 38.10 | 37.66 | 0.63 | 2.06 | 2.88 | 5.24 | 5.44 | 0.28 |
| Exchange | Sorbent | Bare AC Particle | A | 63 | 0.0115 | 24926.04 |  |  |  | 5065.46 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | B | 63 | 0.0115 | 29088.31 | 27007.18 | 2943.17 |  | 6626.15 | 5845.81 | 1103.57 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | A | 63 | 30 | 1.48 |  |  |  | 36.40 |  |  |  |  | 4.93 |  |  |
| Exchange | Water | Bare AC Particle | B | 63 | 30 | 0.77 | 1.13 | 0.50 | 4.38 | 38.12 | 37.26 | 1.21 | 2.20 | 2.93 | 5.029 | 4.98 | 0.07 |
| Exchange | Sorbent | Bare AC Particle | A | 126 | 0.0117 | 24748.38 |  |  |  | 6834.24 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | B | 126 | 0.0115 | 36469.18 | 30608.78 | 8287.86 |  | 6840.43 | 6837.33 | 4.38 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | A | 126 | 30 | 0.78 |  |  |  | 38.16 |  |  |  |  | 5.26 |  |  |
| Exchange | Water | Bare AC Particle | B | 126 | 30 | 1.45 | 1.12 | 0.47 | 4.44 | 39.42 | 38.79 | 0.89 | 2.25 | 2.97 | 5.25 | 5.26 | 0.00 |
| Exchange | Sorbent | Bare AC Particle | A | 187 | 0.0101 | 25481.07 |  |  |  | 7249.31 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | B | 187 | 0.0106 | 23393.02 | 24437.05 | 1476.47 |  | 6389.71 | 6819.51 | 607.82 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | A | 187 | 30 | 0.91 |  |  |  | 40.20 |  |  |  |  | 4.912 |  |  |
| Exchange | Water | Bare AC Particle | B | 187 | 30 | 1.01 | 0.96 | 0.07 | 4.41 | 39.62 | 39.91 | 0.41 | 2.23 | 2.88 | 5.41 | 5.16 | 0.35 |
| Exchange | Sorbent | Bare AC Particle | B | 1397 | 0.0107 | 22189.30 |  |  |  | 14578.29 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | A | 1397 | 0.0108 | 34949.82 | 28569.56 | 9023.05 |  | 13902.54 | 14240.41 | 477.83 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | B | 1397 | 30 | 0.98 |  |  |  | 38.47 |  |  |  |  | 3.83 |  |  |
| Exchange | Water | Bare AC Particle | A | 1397 | 30 | 1.70 | 1.34 | 0.51 | 4.33 | 34.83 | 36.65 | 2.57 | 2.59 | 3.05 | 5.28 | 4.55 | 1.03 |
| Exchange | Sorbent | Bare AC Particle | B | 2875 | 0.0103 | 38280.51 |  |  |  | 18869.22 |  |  |  |  |  |  |  |
| Exchange | Sorbent | Bare AC Particle | A | 2875 | 0.0105 | 28372.35 | 33326.43 | 7006.13 |  | 19557.70 | 19213.46 | 486.83 |  |  |  |  |  |
| Exchange | Water | Bare AC Particle | B | 2875 | 30 | 1.86 |  |  |  | 32.40 |  |  |  |  | 4.39 |  |  |
| Exchange | Water | Bare AC Particle | A | 2875 | 30 | 3.52 | 2.69 | 1.18 | 4.09 | 34.05 | 33.22 | 1.17 | 2.76 | 3.17 | 4.349 | 4.37 | 0.03 |

Table S6

Summary of isotopically labelled MeHgCys:MeHgCys exchange, DOM:Cys exchange, and Cys:DOM exchange experiments data. Samples are broken down by whether they were a part of the uptake or exchange phase, whether the MeHg concentrations were measured in overlying water or polymer material, and by sorbent. Control samples contained MeXXXHgXXX spikes, but no sorbent materials. Averages and standard deviation of MeXXXHg concentrations are shown for triplicate or duplicate treatments at each timepoint.

| Phase | Sample Type | Sorbent | Aqueous Ligand | Replicate | Time (min) | Experiment Course | Mass of Reservoir (g) | Me199Hg (ng/L or ng/kg) | Treatment Avg. Me199Hg | 1 SD | Log(Kps) Me199Hg | Me198Hg (ng/L or ng/kg) | Treatment Avg. Me198Hg | 1 SD | Log(Kps) Me198Hg | Overall Log(Kps) | DOC (mg C/L) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Uptake | Water | Blank | Me199HgCys | A | 20165 | Cys:Cys | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Blank | Me199HgSRHA | B | 20165 | Cys:Cys | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgCys | A | 20165 | Cys:Cys | 40 | 8.73 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgCys | B | 20165 | Cys:Cys | 40 | 8.67 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgCys | C | 20165 | Cys:DOM | 40 | 8.67 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgSRHA | A | 20165 | DOM:Cys | 40 | 8.74 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgSRHA | B | 20165 | DOM:Cys | 40 | 8.79 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | Control | Me199HgSRHA | C | 20165 | DOM:Cys | 40 | 8.76 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | A | 20036 | Cys:Cys | 40 | 0.11 | 0.10 | 0.02 | 3.79 |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | B | 20036 | Cys:Cys | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | C | 20036 | Cys:Cys | 40 | 0.11 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | D | 19952 | Cys:Cys | 40 | 0.13 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | E | 19952 | Cys:Cys | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | F | 20075 | Cys:Cys | 40 | 0.13 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | G | 20075 | Cys:Cys | 40 | 0.14 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | H | 20075 | Cys:Cys | 40 | 0.06 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | I | 20219 | Cys:Cys | 40 | 0.08 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | J | 20219 | Cys:Cys | 40 | 0.07 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | K | 20219 | Cys:Cys | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | L | 20249 | Cys:Cys | 40 | 0.12 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | M | 20249 | Cys:Cys | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | N | 20249 | Cys:Cys | 40 | 0.11 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | O | 20275 | Cys:Cys | 40 | 0.08 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | P | 20219 | Cys:Cys | 40 | 0.06 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | Q | 20219 | Cys:Cys | 40 | 0.08 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | R | 20165 | Cys:Cys | 40 | 0.07 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | S | 20165 | Cys:Cys | 40 | 0.07 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | T | 20165 | Cys:Cys | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | A | 20039 | Cys:DOM | 40 | 0.07 | 0.09 | 0.01 | 3.67 |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | B | 20039 | Cys:DOM | 40 | 0.06 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | C | 19958 | Cys:DOM | 40 | 0.08 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | D | 19958 | Cys:DOM | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | E | 20079 | Cys:DOM | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | F | 20079 | Cys:DOM | 40 | 0.07 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | G | 20223 | Cys:DOM | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | H | 20223 | Cys:DOM | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | I | 20254 | Cys:DOM | 40 | 0.08 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | J | 20254 | Cys:DOM | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | K | 20279 | Cys:DOM | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | L | 20279 | Cys:DOM | 40 | 0.11 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | M | 20165 | Cys:DOM | 40 | 0.09 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgCys | N | 20165 | Cys:DOM | 40 | 0.10 |  |  |  |  |  |  |  |  |  |
| Uptake | Water | ag+AC | Me199HgSRHA | A | 20043 | DOM:Cys | 40 | 4.62 | 4.34 | 0.26 | 1.71 |  |  |  |  |  | 5.801 |
| Uptake | Water | ag+AC | Me199HgSRHA | B | 20043 | DOM:Cys | 40 | 4.11 |  |  |  |  |  |  |  |  | 5.185 |
| Uptake | Water | ag+AC | Me199HgSRHA | C | 19965 | DOM:Cys | 40 | 4.15 |  |  |  |  |  |  |  |  | 5.542 |
| Uptake | Water | ag+AC | Me199HgSRHA | D | 19965 | DOM:Cys | 40 | 4.48 |  |  |  |  |  |  |  |  | 5.699 |
| Uptake | Water | ag+AC | Me199HgSRHA | E | 20083 | DOM:Cys | 40 | 4.29 |  |  |  |  |  |  |  |  | 5.574 |
| Uptake | Water | ag+AC | Me199HgSRHA | F | 20083 | DOM:Cys | 40 | 4.24 |  |  |  |  |  |  |  |  | 5.176 |
| Uptake | Water | ag+AC | Me199HgSRHA | G | 20227 | DOM:Cys | 40 | 4.19 |  |  |  |  |  |  |  |  | 5.532 |
| Uptake | Water | ag+AC | Me199HgSRHA | H | 20227 | DOM:Cys | 40 | 4.04 |  |  |  |  |  |  |  |  | 5.421 |
| Uptake | Water | ag+AC | Me199HgSRHA | I | 20258 | DOM:Cys | 40 | 4.40 |  |  |  |  |  |  |  |  | 5.518 |
| Uptake | Water | ag+AC | Me199HgSRHA | J | 20258 | DOM:Cys | 40 | 4.07 |  |  |  |  |  |  |  |  | 5.534 |
| Uptake | Water | ag+AC | Me199HgSRHA | K | 20283 | DOM:Cys | 40 | 4.40 |  |  |  |  |  |  |  |  | 5.569 |
| Uptake | Water | ag+AC | Me199HgSRHA | L | 20283 | DOM:Cys | 40 | 4.20 |  |  |  |  |  |  |  |  | 5.387 |
| Uptake | Water | ag+AC | Me199HgSRHA | M | 20165 | DOM:Cys | 40 | 4.83 |  |  |  |  |  |  |  |  | 5.540 |
| Uptake | Water | ag+AC | Me199HgSRHA | N | 20165 | DOM:Cys | 40 | 4.81 |  |  |  |  |  |  |  |  | 5.579 |
| Uptake | Polymer | ag+AC | Me199HgCys | R | 20165 | Cys:Cys | 0.74 | 476.80 | 472.01 | 15.40 |  |  |  |  |  |  |  |
| Uptake | Polymer | ag+AC | Me199HgCys | S | 20165 | Cys:Cys | 0.73 | 484.46 |  |  |  |  |  |  |  |  |  |
| Uptake | Polymer | ag+AC | Me199HgCys | T | 20165 | Cys:Cys | 0.78 | 454.78 |  |  |  |  |  |  |  |  |  |
| Uptake | Polymer | ag+AC | Me199HgCys | N | 20165 | Cys:DOM | 0.73 | 479.74 | 479.74 | NA |  |  |  |  |  |  |  |
| Uptake | Polymer | ag+AC | Me199HgSRHA | M | 20165 | DOM:Cys | 0.81 | 215.42 | 220.31 | 6.92 |  |  |  |  |  |  |  |
| Uptake | Polymer | ag+AC | Me199HgSRHA | N | 20165 | DOM:Cys | 0.78 | 225.21 |  |  |  |  |  |  |  |  |  |
| Exchange | Water | Blank | Me198HgCys | A | 20165 | Experiment | 40 | 0.00 |  |  |  | 0.00 |  |  |  |  |  |
| Exchange | Water | Control | Me198HgCys | A | 20165 | Experiment | 40 | -0.01 |  |  |  | 18.64 |  |  |  |  |  |
| Exchange | Water | Control | Me198HgCys | B | 20165 | Experiment | 40 | 0.01 |  |  |  | 18.47 |  |  |  |  |  |
| Exchange | Water | Control | Me198HgCys | C | 20165 | Experiment | 40 | 0.00 |  |  |  | 18.73 |  |  |  |  |  |
| Exchange | Water | Blank | SRHA, no MeHg | A | 20165 | Experiment | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Exchange | Water | Control | SRHA, no MeHg | B | 20165 | Experiment | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Exchange | Water | Control | L-Cys, no MeHg | A | 20165 | Experiment | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Exchange | Water | Control | L-Cys, no MeHg | B | 20165 | Experiment | 40 | 0.00 |  |  |  |  |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | A | 63 | Cys:Cys | 40 | 0.04 | 0.03 | 0.01 | 4.14 | 16.06 | 16.13 | 0.14 | 0.88 | 1.53 |  |
| Exchange | Water | ag+AC | Me198HgCys | B | 64 | Cys:Cys | 40 | 0.03 |  |  |  | 16.30 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | C | 65 | Cys:Cys | 40 | 0.02 |  |  |  | 16.03 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | D | 364 | Cys:Cys | 40 | 0.04 | 0.04 | 0.01 | 3.99 | 12.11 | 12.33 | 0.35 | 1.43 | 1.80 |  |
| Exchange | Water | ag+AC | Me198HgCys | E | 365 | Cys:Cys | 40 | 0.06 |  |  |  | 12.74 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | F | 367 | Cys:Cys | 40 | 0.04 |  |  |  | 12.14 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | G | 1434 | Cys:Cys | 40 | 0.07 | 0.08 | 0.02 | 3.72 | 5.87 | 5.16 | 0.67 | 2.09 | 2.30 |  |
| Exchange | Water | ag+AC | Me198HgCys | H | 1435 | Cys:Cys | 40 | 0.10 |  |  |  | 4.54 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | I | 1436 | Cys:Cys | 40 | 0.06 |  |  |  | 5.09 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | J | 2581 | Cys:Cys | 40 | 0.09 | 0.08 | 0.01 | 3.71 | 1.88 | 2.34 | 0.41 | 2.57 | 2.73 |  |
| Exchange | Water | ag+AC | Me198HgCys | K | 2582 | Cys:Cys | 40 | 0.07 |  |  |  | 2.46 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | L | 2583 | Cys:Cys | 40 | 0.10 |  |  |  | 2.67 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | M | 10101 | Cys:Cys | 40 | 0.08 | 0.08 | 0.01 | 3.69 | 0.33 | 0.37 | 0.05 | 3.38 | 3.45 |  |
| Exchange | Water | ag+AC | Me198HgCys | N | 10103 | Cys:Cys | 40 | 0.07 |  |  |  | 0.37 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | O | 10105 | Cys:Cys | 40 | 0.09 |  |  |  | 0.42 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | P | 20104 | Cys:Cys | 40 | 0.06 | 0.06 | 0.01 | 3.78 | 0.25 | 0.30 | 0.05 | 3.47 | 3.54 |  |
| Exchange | Water | ag+AC | Me198HgCys | Q | 20161 | Cys:Cys | 40 | 0.08 |  |  |  | 0.34 |  |  |  |  |  |
| Exchange | Water | ag+AC | Me198HgCys | R | 20163 | Cys:Cys | 40 | 0.05 |  |  |  | 0.29 |  |  |  |  |  |
| Exchange | Water | ag+AC | SRHA, no MeHg | A | 64 | Cys:DOM | 40 | 0.12 | 0.10 | 0.03 | 3.58 |  |  |  |  |  | 9.290 |
| Exchange | Water | ag+AC | SRHA, no MeHg | B | 66 | Cys:DOM | 40 | 0.09 |  |  |  |  |  |  |  |  | 9.441 |
| Exchange | Water | ag+AC | SRHA, no MeHg | C | 363 | Cys:DOM | 40 | 0.17 | 0.17 | 0.01 | 3.38 |  |  |  |  |  | 8.427 |
| Exchange | Water | ag+AC | SRHA, no MeHg | D | 366 | Cys:DOM | 40 | 0.17 |  |  |  |  |  |  |  |  | 8.452 |
| Exchange | Water | ag+AC | SRHA, no MeHg | E | 1434 | Cys:DOM | 40 | 0.38 | 0.37 | 0.02 | 3.05 |  |  |  |  |  | 7.392 |
| Exchange | Water | ag+AC | SRHA, no MeHg | F | 1436 | Cys:DOM | 40 | 0.36 |  |  |  |  |  |  |  |  | 7.641 |
| Exchange | Water | ag+AC | SRHA, no MeHg | H | 2581 | Cys:DOM | 40 | NA | 0.48 | 0.00 | 2.92 |  |  |  |  |  | 7.264 |
| Exchange | Water | ag+AC | SRHA, no MeHg | H | 2583 | Cys:DOM | 40 | 0.48 |  |  |  |  |  |  |  |  | 7.227 |
| Exchange | Water | ag+AC | SRHA, no MeHg | I | 10102 | Cys:DOM | 40 | 0.95 | 0.96 | 0.01 | 2.62 |  |  |  |  |  | 6.06 |
| Exchange | Water | ag+AC | SRHA, no MeHg | J | 10104 | Cys:DOM | 40 | 0.97 |  |  |  |  |  |  |  |  | 5.27 |
| Exchange | Water | ag+AC | SRHA, no MeHg | K | 20105 | Cys:DOM | 40 | 1.34 | 1.36 | 0.03 | 2.41 |  |  |  |  |  | 5.40 |
| Exchange | Water | ag+AC | SRHA, no MeHg | L | 20106 | Cys:DOM | 40 | 1.38 |  |  |  |  |  |  |  |  | 5.85 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | A | 64 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 1.06 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | B | 66 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 0.71 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | C | 361 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 0.77 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | D | 363 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 0.79 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | E | 1434 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 0.88 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | F | 1436 | DOM:Cys | 40 | NA |  |  |  |  |  |  |  |  | 0.88 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | G | 2580 | DOM:Cys | 40 | 0.12 | 0.12 | 0.01 | 3.24 |  |  |  |  |  | 1.11 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | H | 2582 | DOM:Cys | 40 | 0.13 |  |  |  |  |  |  |  |  | 1.05 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | I | 10101 | DOM:Cys | 40 | 0.14 | 0.14 | 0.00 | 3.17 |  |  |  |  |  | 1.15 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | J | 10103 | DOM:Cys | 40 | 0.14 |  |  |  |  |  |  |  |  | 0.90 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | K | 20104 | DOM:Cys | 40 | 0.14 | 0.13 | 0.02 | 3.22 |  |  |  |  |  | 1.01 |
| Exchange | Water | ag+AC | L-Cys, no MeHg | L | 20106 | DOM:Cys | 40 | 0.11 |  |  |  |  |  |  |  |  | 0.76 |
| Exchange | Polymer | ag+AC | Me198HgCys | A | 63 | Cys:Cys | 0.83 | 426.15 | 429.27 | 22.08 |  | 128.01 | 122.48 | 5.08 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | B | 64 | Cys:Cys | 0.87 | 408.92 |  |  |  | 118.01 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | C | 65 | Cys:Cys | 0.81 | 452.75 |  |  |  | 121.43 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | D | 364 | Cys:Cys | 0.80 | 439.01 | 438.05 | 17.81 |  | 347.49 | 333.90 | 12.87 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | E | 365 | Cys:Cys | 0.78 | 455.36 |  |  |  | 332.32 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | F | 367 | Cys:Cys | 0.86 | 419.79 |  |  |  | 321.88 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | G | 1434 | Cys:Cys | 0.92 | 383.57 | 395.02 | 15.62 |  | 588.79 | 638.88 | 49.88 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | H | 1435 | Cys:Cys | 0.86 | 412.82 |  |  |  | 688.55 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | I | 1436 | Cys:Cys | 0.87 | 388.68 |  |  |  | 639.28 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | J | 2581 | Cys:Cys | 0.83 | 423.74 | 436.20 | 10.84 |  | 874.07 | 864.91 | 8.25 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | K | 2582 | Cys:Cys | 0.80 | 443.51 |  |  |  | 858.07 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | L | 2583 | Cys:Cys | 0.80 | 441.34 |  |  |  | 862.58 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | M | 10101 | Cys:Cys | 0.85 | 400.64 | 389.90 | 11.66 |  | 915.01 | 883.15 | 32.15 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | N | 10103 | Cys:Cys | 0.88 | 391.58 |  |  |  | 883.73 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | O | 10105 | Cys:Cys | 0.87 | 377.49 |  |  |  | 850.72 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | P | 20104 | Cys:Cys | 0.96 | 349.72 | 381.78 | 61.31 |  | 805.21 | 876.67 | 139.93 |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | Q | 20161 | Cys:Cys | 0.78 | 452.47 |  |  |  | 1037.90 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | Me198HgCys | R | 20163 | Cys:Cys | 1.00 | 343.14 |  |  |  | 786.89 |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | A | 64 | Cys:DOM | 0.83 | 416.01 | 396.87 | 27.07 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | B | 66 | Cys:DOM | 0.86 | 377.73 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | C | 363 | Cys:DOM | 0.79 | 428.04 | 405.34 | 32.10 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | D | 366 | Cys:DOM | 0.86 | 382.65 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | E | 1434 | Cys:DOM | 0.80 | 408.70 | 414.18 | 7.74 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | F | 1436 | Cys:DOM | 0.79 | 419.65 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | G | 2581 | Cys:DOM | 0.78 | 409.58 | 401.49 | 11.44 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | H | 2583 | Cys:DOM | 0.83 | 393.40 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | I | 10102 | Cys:DOM | 0.81 | 386.19 | 396.49 | 14.56 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | J | 10104 | Cys:DOM | 0.79 | 406.79 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | K | 20105 | Cys:DOM | 0.80 | 338.37 | 349.22 | 15.34 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | SRHA, no MeHg | L | 20106 | Cys:DOM | 0.81 | 360.07 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | A | 64 | DOM:Cys | 0.83 | 200.11 | 206.33 | 8.80 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | B | 66 | DOM:Cys | 0.79 | 212.55 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | C | 361 | DOM:Cys | 0.80 | 207.29 | 201.58 | 8.09 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | D | 363 | DOM:Cys | 0.78 | 195.86 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | E | 1434 | DOM:Cys | 0.80 | 206.11 | 202.34 | 5.33 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | F | 1436 | DOM:Cys | 0.87 | 198.57 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | G | 2580 | DOM:Cys | 0.80 | 200.82 | 211.83 | 15.57 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | H | 2582 | DOM:Cys | 0.74 | 222.84 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | I | 10101 | DOM:Cys | 0.83 | 204.54 | 204.03 | 6.39 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | J | 10103 | DOM:Cys | 0.82 | 206.16 |  |  |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | K | 20104 | DOM:Cys | 0.78 | 199.51 | 205.35 | 1.14 |  |  |  |  |  |  |  |
| Exchange | Polymer | ag+AC | L-Cys, no MeHg | L | 20106 | DOM:Cys | 0.80 | 208.56 |  |  |  |  |  |  |  |  |  |

Table S7

Kinetic parameters obtained from fitting time-series data to a first-order adsorption model with equilibrium exchange.

|  | kdesorb (d-1) | (R2)desorb | -kadsorp (d-1) | (R2)adsorb | kadsorb:kdesorb | 199t90 | 198t90 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MeHgSRHA | -0.046 | 0.86 | -0.057 | 0.52 | 1.23 | 34.56 | 28.00 |
| MeHgCys | -0.0126 | 1.00 | -0.0197 | 0.98 | 1.57 | 2.48 | 1.58 |

Table S8

Full crosstab of analyte concentrations in passive sampler (ps) portions in the sediment (ps-sed) and in the overlying water (ps-water), sediment (sed), overlying water (w), and porewater (pw). Sulfide concentrations below detection limit of 0.5 µM have been denoted “< 0.5.” Partitioning coefficients calculated are expressed as the log transform of the aqueous concentration in ng/L divided by the solid concentration in ng/kg. MeHg concentrations in a quality control blank were measured in the aqueous phase at t0, t+7, t+14, and t+21 and in a passive sampler at t+21 in a jar filled with plain DI water.

| Sample Type | Rep | Time Point | Csed (ng/kg) | Cw (ng/L) | Cpw (ng/L) | Cps-water (ng/kg) | Cps-sed (ng/kg) | Sed:Water log Kd | log Kps:pw | log Kps:w | [S2-]w (µM) | pHw | DOCw (mg/L) | [Cl-]w (mM) | [SO42-]w (mM) | [S2-]pw (µM) | pHpw | DOCpw (mg/L) | [Cl-]pw (mM) | [SO42-]pw (mM) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| no-ps | a | t-14 | 121022 | 1.72 | 24.69 |  |  | 3.69 |  |  | 0.57 | 7.11 | 8.53 | 42.17 | 1.81 | 3.45 | 7.2 | 37.68 | 55.91 | 0.49 |
| no-ps | b | t-14 | 102228 | 0.83 | 18.18 |  |  | 3.75 |  |  | < 0.5 | 6.98 | 6.96 | 33.23 | 1.45 | 2.40 | 7.29 | 39.67 | 83.80 | 0.61 |
| no-ps | c | t-14 | 85646 | 0.65 | 15.88 |  |  | 3.73 |  |  | < 0.5 | 7.18 | 6.65 | 53.94 | 2.03 | 1.86 | 7.3 | 41.80 | 66.42 | 0.46 |
| no-ps | a | t0 | 172409 | 1.45 | 41.45 |  |  | 3.62 |  |  | < 0.5 | 7.82 | 17.21 | 33.37 | 0.80 | 2.50 | 6.95 |  | 69.27 | 1.80 |
| no-ps | b | t0 | 111192 | 1.44 | 23.07 |  |  | 3.68 |  |  | 0.53 | 7.84 | 18.91 | 39.89 | 0.88 | 1.40 | 7.06 | 41.54 | 67.38 | 1.56 |
| no-ps | c | t0 | 136289 | 1.11 | 20.05 |  |  | 3.83 |  |  | < 0.5 | 7.55 | 18.47 | 26.47 | 0.63 | 1.16 | 6.92 | 38.90 | 54.84 | 1.31 |
| no-ps | a | t+7 | 171671 | 0.81 | 31.57 |  |  | 3.74 |  |  | 0.61 | 7.41 | 17.60 | 71.50 | 2.43 | 4.45 | 6.86 | 23.78 | 66.82 | 2.31 |
| no-ps | b | t+7 | 112522 | 0.99 | 31.06 |  |  | 3.56 |  |  | 0.52 | 7.57 | 17.85 | 62.46 | 1.93 | 3.83 | 6.84 | 22.90 | 65.86 | 2.01 |
| no-ps | c | t+7 | 114789 | 0.76 | 28.18 |  |  | 3.61 |  |  | < 0.5 | 7.64 | 16.91 | 60.43 | 1.92 | 2.84 | 6.79 | 25.34 | 59.49 | 1.76 |
| sheet-ps | a | t+7 | 135573 | 0.80 | 21.95 | 369 | 52339 | 3.79 | 3.38 | 2.67 | < 0.5 | 7.6 | 16.01 | 63.14 | 1.91 | 1.46 | 6.92 | 30.98 | 62.00 | 1.85 |
| sheet-ps | b | t+7 | 147547 | 1.07 | 20.67 | 223 | 25912 | 3.85 | 3.10 | 2.32 | < 0.5 | 7.67 | 14.31 | 59.70 | 1.82 | 2.15 | 6.81 | 24.34 | 63.11 | 1.96 |
| sheet-ps | c | t+7 | 101852 | 1.13 | 13.62 | 314 | 39722 | 3.87 | 3.46 | 2.44 | < 0.5 | 7.59 | 13.32 | 63.38 | 2.00 | 0.99 | 6.96 | 19.94 | 60.63 | 1.86 |
| no-ps | a | t+14 | 79485 | 0.63 | 17.96 |  |  | 3.65 |  |  | < 0.5 | 7.84 | 18.32 | 42.42 | 1.23 | 1.70 | 6.59 | 22.87 | 57.51 | 1.83 |
| no-ps | b | t+14 | 37434 | 0.78 | 14.75 |  |  | 3.40 |  |  | < 0.5 | 7.92 | 16.66 | 46.02 | 1.23 | 1.38 | 6.61 | 23.38 | 59.22 | 2.04 |
| no-ps | c | t+14 | 152607 | 1.19 | 15.68 |  |  | 3.99 |  |  | < 0.5 | 7.97 | 18.02 | 50.76 | 1.40 | 1.28 | 6.67 | 22.73 | 61.78 | 1.91 |
| sheet-ps | a | t+14 | 97909 | 0.70 | 18.89 | 163 | 16800 | 3.71 | 2.95 | 2.37 | < 0.5 | 8.04 | 13.61 | 48.37 | 1.54 | 1.82 | 6.5 | 18.23 | 67.55 | 2.64 |
| sheet-ps | b | t+14 | 217431 | 0.64 | 16.35 |  | 25059 | 4.12 | 3.19 |  | < 0.5 | 8 | 12.08 | 46.19 | 1.27 | 1.14 | 6.59 | 18.95 | 72.99 | 2.51 |
| sheet-ps | c | t+14 | 151360 | 0.53 | 19.47 | 302 | 15155 | 3.89 | 2.89 | 2.75 | < 0.5 | 8 | 13.13 | 65.04 | 2.68 | 1.61 | 6.58 | 22.48 | 71.23 | 2.94 |
| split-ps | a | t+14 | 111161 | 0.53 | 19.36 | 248 |  | 3.76 |  | 2.67 | < 0.5 | 7.94 | 13.35 | 74.01 | 2.56 | 2.18 | 6.5 | 17.37 | 123.93 | 4.49 |
| split-ps | b | t+14 | 114571 | 0.63 | 19.59 | 294 | 24450 | 3.77 | 3.10 | 2.67 | < 0.5 | 7.99 | 14.21 | 48.12 | 1.31 | 1.43 | 6.55 | 17.92 | 59.68 | 2.25 |
| split-ps | c | t+14 | 108326 | 0.61 | 18.21 | 230 | 18315 | 3.77 | 3.00 | 2.58 | < 0.5 | 7.98 | 13.07 | 39.40 | 1.01 | 1.14 | 6.53 | 17.73 | 57.59 | 2.04 |
| no-ps | a | t+21 | 136416 | 0.61 | 10.23 |  |  | 4.12 |  |  | < 0.5 | 7.58 | 16.57 | 58.97 | 2.17 | 1.32 | 6.59 | 19.87 | 64.53 | 2.51 |
| no-ps | b | t+21 | 169021 | 0.57 | 16.88 |  |  | 4.00 |  |  | < 0.5 | 7.56 | 13.15 | 46.38 | 1.21 | 2.48 | 6.72 | 17.84 | 62.42 | 2.09 |
| no-ps | c | t+21 | 107749 | 0.70 | 6.53 |  |  | 4.22 |  |  | < 0.5 | 7.71 | 13.37 | 39.01 | 0.92 | 1.02 | 6.8 | 17.97 | 63.49 | 2.15 |
| sheet-ps | a | t+21 | 105134 | 0.60 | 14.60 | 688 | 14231 | 3.86 | 2.99 | 3.06 | < 0.5 | 7.76 | 13.86 | 72.85 | 3.09 | 1.30 | 6.75 | 18.81 | 72.18 | 3.11 |
| sheet-ps | b | t+21 | 75585 | 0.55 | 9.98 | 377 | 34971 | 3.88 | 3.54 | 2.84 | < 0.5 | 7.89 | 13.17 | 71.18 | 2.83 | 1.22 | 6.74 | 18.65 | 66.11 | 2.67 |
| sheet-ps | c | t+21 | 205552 | 0.31 | 14.97 | 254 | 33364 | 4.14 | 3.35 | 2.91 | < 0.5 | 7.95 | 11.67 | 71.72 | 2.71 | 2.27 | 6.77 | 17.00 | 70.91 | 2.72 |
| split-ps | a | t+21 | 112685 | 0.49 | 14.66 | 327 | 40540 | 3.89 | 3.44 | 2.83 | < 0.5 | 7.86 | 11.50 | 22.58 | 0.62 | 2.21 | 6.75 | 14.39 | 66.16 | 2.13 |
| split-ps | b | t+21 | 110577 | 0.50 | 13.63 | 343 | 45227 | 3.91 | 3.52 | 2.83 | < 0.5 | 7.93 | 11.49 | 27.72 | 0.87 | 1.76 | 6.73 | 14.02 | 69.04 | 2.54 |
| split-ps | c | t+21 | 126309 | 0.41 | 9.80 | 198 | 39682 | 4.11 | 3.61 | 2.68 | < 0.5 | 7.91 | 9.95 | 56.22 | 2.02 | 1.20 | 6.7 | 13.19 | 66.60 | 2.44 |
| blank | - | t0 |  | 0.03 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| blank | - | t+7 |  | 0.03 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| blank | - | t+14 |  | 0.16 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| blank-ps | - | t+21 |  | -0.01 |  | 7.22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Table S9. Equilibrium constants used for modeling MeHg speciation in sediment:water microcosms.

| educts |  |  | products |  | Species | Notes | Log Kf | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H20 |  | <==> | OH- | H+ | OH- | for 25˚ C | 14.0 | NIST Critical |
| Sulfide protonation |  |  |  |  |  |  |  |  |
| H2S |  | <==> | HS- | H+ | HS- |  | 7.0 | Millero 1986; NIST Critical |
| HS- |  | <==> | S2- | H+ |  |  | 13.9 | Smith and Martell 1976 |
| Thiol protonation |  |  |  |  |  |  |  |  |
| RS- | H+ | <==> | RSH |  | cysteine | value for cysteine | 8.6 | Liem-Nguyen 2017; Skyllberg 2003 |
| NOM-RS | H+ | <==> | NOM-RSH |  | LMM thiols |  | 9.0 | Jalilehvand 2013 |
| Aquo MeHg compounds |  |  |  |  |  |  |  |  |
| MeHg+ | H2O | <==> | MeHgOH | H+ | MeHgOH |  | -4.8 | Loux 2007; DeRobertis et al. (1998) |
| 2(MeHg+) | H2O | <==> | (MeHg)2OH+ |  | (MeHg)2OH+ |  | -2.3 | Loux 2007; DeRobertis et al. (1998) |
| MeHg+ | Cl- | <==> | MeHgCl |  | MeHgCl |  | 5.4 | Loux 2007; DeRobertis et al. (1998) |
| MeHg+ | HS- | <==> | MeHgSH |  | MeHgSH |  | 14.5 | Dyrssen and Wedborg 1991 |
| MeHg+ | HS- | <==> | MeHgS- | H+ | MeHgS- |  | 7.00 | Schwarzenbach and Schellenberg 1965 |
| 2MeHg+ | HS- | <==> | (MeHg)2S | H+ | (MeHg)2S |  | 26.0 | Kanzler et al 2018 |
| MeHg+ | RS- | <==> | MeHgRS |  | MeHgRS | values for cysteine | 15.7 | Loux 2007; Friedman 1973 |
|  |  |  |  |  |  |  | 15.7-17.5 | Liem Nguyen 2017; Reid et al 1981 |
| MeHg+ | NOM-RS- | <==> | MeHg(NOM-RS) |  | MeHg(NOM-RS) |  | 16.3-16.7 | Qian 2002 |
|  |  |  |  |  |  |  | 15.6-17.1 | Karlsson and Skyllberg 2003 |