Support Information

## Analysis of the steady-state concentrations of reactive species and their role in contaminant degradation by the iron-biochar/ persulfate advanced oxidation process: comparison of probe compound and quenching agent methods

## Xukun Meng1, Guilong Peng1,6,*, Yuting Yan1, Xiao Wang1, Jiangwei Zhu2, Carolina Belver3, Wenwen Gong4,*, Lee Blaney5,*

1State Key Laboratory of Resource Insects,
College of Sericulture, Textile and Biomass Sciences, Southwest University,

Chongqing, 400715, China

2Co-Innovation Center for Sustainable Forestry in Southern China,
Nanjing Forestry University, Nanjing 210037, China

3Chemical Engineering Department, Universidad Autónoma de Madrid, Campus Cantoblanco, E-28049 Madrid, Spain

4Institute of Quality Standard and Testing Technology, Beijing Academy of Agriculture and Forestry Science, Beijing 100097, China

5University of Maryland Baltimore County, Department of Chemical, Biochemical, and Environmental Engineering, Baltimore, MD 21250, USA

6Yibin Academy of Southwest University, Yibin, China

*Corresponding authors’ email:

gong_ww@126.com (W. Gong)

blaney@umbc.edu (L. Blaney)

pengguilong@swu.edu.cn (G. Peng)

Text S1

Calculation of steady-state concentrations of •OH, SO4•−, 1O2, and O2•–

The BA, NB, p-CBA, and FFA probe compounds were added to experimental solutions being treated by the Fe-BC/PS system. A mass balance was written for each probe compound (Eq. S1-S4) [1].

dNBdt=-k•OH,NB″•OHNB	(Eq. S1)

dBAdt=-k•OH,BA″•OH+kSO4•–,BA″SO4•–[BA]	(Eq. S2)

dFFAdt=-k•OH,FFA″•OH+kSO4•–,FFA″SO4•–+k1O2,FFA″[1O2]+kO2•–,FFA″[O2•–]FFA	(Eq. S3)

dp‐CBAdt=-k•OH,p‐CBA″•OH+kSO4•–,p‐CBA″SO4•–+k1O2,p‐CBA″[1O2]+kO2•–,p‐CBA″[O2•–]p‐CBA	(Eq. S4)

Integrating Eq. S1-S4 yields Eq. S5-S8.

lnNBNB0=-k•OH,NB″•OHss t=-kobs,NB' t	(Eq. S5)

lnBABA0=-k•OH,BA″•OHss+kSO4•–,BA″SO4•–sst=-kobs,BA' t	(Eq. S6)

lnFFAFFA0=-k•OH,FFA″•OHss+kSO4•–,FFA″SO4•–ss+k1O2,FFA″1O2ss+kO2•–,FFA″O2•–sst=-kobs,FFA' t	(Eq. S7)

lnp‐CBAp‐CBA0=-k•OH,p‐CBA″•OHss+kSO4•–,p‐CBA″SO4•–ss+k1O2,p‐CBA″1O2ss+kO2•–,p‐CBA″O2•–sst=-kobs,p‐CBA' t	(Eq. S8)

The steady-state concentrations of •OH ([•OH]ss) and SO4•– ([SO4•–]ss) were obtained from Eq. S9 and Eq. S10, respectively.

•OHss=kobs,NB'k•OH,NB″	(Eq. S9)

SO4•–ss=kobs,BA'-k•OH,BA″•OHsskSO4•–,BA″	(Eq. S10)

The steady-state concentrations of 1O2 ([1O2]ss) and O2•‐ ([O2•‐]ss) were calculated with Eq. S11 and S12, respectively.

1O2ss=kobs,FFA'-k•OH,FFA″•OHss+kSO4•–,FFA″SO4•–ssk1O2,FFA″	(Eq. S11)

O2•–ss=kobs,p‐CBA'-k•OH,p‐CBA″•OHss+kSO4•–,p‐CBA″SO4•–ss+k1O2,p‐CBA″1O2sskO2•–,p‐CBA″	(Eq. S12)

In Eq. S1-S12, [NB]0, [BA]0, [FFA]0, and [p-CBA]0 represent the initial concentrations of NB, BA, FFA, and p-CBA, respectively, [NB], [BA], [FFA], and [p-CBA] represent the concentration of NB, BA, FFA, and p-CBA at time t, respectively, kobs,NB', kobs,BA', kobs,FFA', and kobs,p‐CBA' are the pseudo-first-order rate constants for degradation of NB, BA, FFA, and p-CBA, respectively, k•OH,NB″ is the second-order rate constant for reaction of NB with •OH, k•OH,BA″ and kSO4•–,BA″ are the second-order rate constants for reaction of BA with •OH and SO4•–, respectively, k•OH,FFA″, kSO4•–,FFA″, k1O2,FFA″, and kO2•–,FFA″ are the second-order rate constants for reaction of FFA with •OH, SO4•−, 1O2, and O2•–, respectively, and k•OH,p‐CBA″, kSO4•–,p‐CBA″, k1O2,p‐CBA″, and kO2•–,p‐CBA″ are the second-order rate constants for reaction of p-CBA with •OH, SO4•−, 1O2, and O2•–, respectively.

As an alternative approach, the steady-state concentration of O2•– was determined using the p-BQ probe compound (Eq. S13) with addition of 500 mM MeOH in the reaction system to quench •OH and SO4•−.

lnp‐BQp‐BQ0=-kO2•–,p‐BQ″O2•–ss+k1O2,p‐BQ″1O2ss t=-kobs,p‐BQ' t	(Eq. S13)

Then, the steady-state concentration O2•– can be obtained from Eq. S14.

O2•–ss=kobs,p‐BQ'-k1O2,p‐BQ″1O2sskO2•–,p‐BQ″	(Eq. S14)

In the presence of the MeOH quenching agent, which scavenges •OH and SO4•−, the steady-state concentration of 1O2 from Eq. S11 can be simplified to Eq. S15.

1O2ss=kobs,FFA'k1O2,FFA″	(Eq. S15)

In the absence of the MeOH quenching agent, the steady-state concentration of O2•– can be calculated via Eq. S16.

O2•–ss=kobs,p‐BQ'-k•OH,p‐BQ″•OHss+kSO4•–,p‐BQ″SO4•–ss+k1O2,p‐BQ″1O2sskO2•–,p‐BQ″	(Eq. S16)

Contribution of each reactive species to sulfamethoxazole degradation

The observed rate constants for sulfamethoxazole and the probe compounds can be written as shown in Eq. S17-S21.

kobs,SMX'=k•OH,SMX'+kSO4•–,SMX'+k1O2,SMX'+kO2•–,SMX'+kFe(IV),SMX'	(Eq. S17)

k•OH,SMX'=k•OH,SMX″•OHss	(Eq. S18)

kSO4•–,SMX'=kSO4•–,SMX″SO4•–ss	(Eq. S19)

k1O2,SMX'=k1O2,SMX″1O2ss	(Eq. S20)

kO2•–,SMX'=kO2•–,SMX″O2•–ss	(Eq. S21)

Substituting Eq. S18-S21 into Eq. S17, the relative contributions of •OH, SO4•−, 1O2, and Fe(IV) to sulfamethoxazole degradation can be determined (Eq. S22-S26).

R•OH=k•OH,SMX″[•OH]sskobs,SMX'×100%	(Eq. S22)

RSO4•–=kSO4•–,SMX″[SO4•–]sskobs,SMX'×100%	(Eq. S23)

R1O2=k1O2,SMX″[1O2]sskobs,SMX'×100%	(Eq. S24)

RO2•–=kO2•–,SMX″[O2•–]sskobs,SMX'×100%	(Eq. S25)

RFe(IV)=100-R•OH-RSO4•–-R1O2-RO2•–	(Eq. S26)

The pseudo-first-order rate constant for sulfamethoxazole reaction with Fe(IV) can be determined by rearranging Eq. S17 to Eq. S27. Then, the corresponding second-order rate constant can be determined from Eq. S28.

kFe(IV),SMX'=kobs,SMX'-k•OH,SMX'+kSO4•–,SMX'+k1O2,SMX'+kO2•–,SMX'	(Eq. S27)

kFe(IV),SMX″=kFe(IV),SMX'[Fe(IV)]ss	(Eq. S28)

Table S1. Operating parameters for single-solute analysis of sulfamethoxazole and probe compounds by HPLC.

| Compound | Mobile phase |  |  | Wavelength (nm) |
| --- | --- | --- | --- | --- |
|  | Water with 0.2% acetic acid (%) | Methanol (%) | Flow rate (mL/min) |  |
| BA | 40 | 60 | 1.0 | 227 |
| NB | 40 | 60 | 1.0 | 270 |
| p-BQ | 20 | 80 | 1.0 | 254 |
| p-CBA | 20 | 80 | 1.0 | 234 |
| Sulfamethoxazole | 40 | 60 | 1.0 | 270 |
| Compound | Mobile phase |  |  | Wavelength (nm) |
|  | Water with 0.2% acetic acid (%) | Acetonitrile (%) | Flow rate (mL/min) |  |
| PMSO | 50 | 50 | 1.0 | 235 |
| PMSO2 | 50 | 50 | 1.0 | 215 |

Table S2. Mobile-phase gradient for multi-solute analysis of sulfamethoxazole and probe compounds by HPLC.

| Time (min) | Water with 0.2% acetic acid (%) | Methanol (%) | Flow rate (mL/min) |
| --- | --- | --- | --- |
| 0.0 | 55 | 45 | 1.0 |
| 5.0 | 55 | 45 | 1.0 |
| 10.0 | 85 | 15 | 1.0 |
| 15.0 | 55 | 45 | 1.0 |

Table S3. Steady-state concentrations of •OH and SO4•− calculated from solutions that contained sulfamethoxazole and the NB or BA probe compounds (one probe present in each solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,NB' (s-1) | 2.0 10-3 | 1.6 10-3 | 1.2 10-3 |
| kobs,BA' (s-1) | 1.6 10-3 | 1.3 10-3 | 1.1 10-3 |
| •OHss (M) | 5.13 10-13 | 4.10 10-13 | 3.08 10-13 |
| SO4•–ss (M) | 1.69 10-13 | 1.37 10-13 | 1.24 10-13 |

Table S4. Steady-state concentrations of •OH and SO4•− calculated from solutions that contained sulfamethoxazole and the NB and BA probe compounds (both probes present in same solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,NB' (s-1) | 1.2 10-3 | 9.16 10-4 | 9.00 10-4 |
| kobs,BA' (s-1) | 1.3 10-3 | 9.55 10-4 | 5.85 10-4 |
| •OHss (M) | 3.08 10-13 | 2.35 10-13 | 2.31 10-13 |
| SO4•–ss (M) | 1.58 10-13 | 1.14 10-13 | 5.20 10-14 |

Table S5. Steady-state concentrations of •OH, SO4•−, 1O2, and O2•– calculated from solutions that contained sulfamethoxazole and the NB, BA, FFA, and p-CBA probe compounds (all probes present in same solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,NB' (s-1) | 6.19 10-4 | 5.32 10-4 | 3.50 10-4 |
| kobs,BA' (s-1) | 8.77 10-4 | 3.57 10-4 | 2.12 10-4 |
| kobs,FFA' (s-1) | 2.11 10-2 | 1.15 10-3 | 5.75 10-4 |
| kobs,p‐CBA' (s-1) | 2.34 10-3 | 1.02 10-3 | 5.43 10-4 |
| •OHss (M) | 1.59 10-13 | 1.36 10-13 | 8.97 10-14 |
| SO4•–ss (M) | 1.16 10-13 | 3.28 10-14 | 1.77 10-14 |
| 1O2ss (M) | 1.39 10-10 | - a | - a |
| O2•–ss (M) | - a | - a | - a |

a: this parameter could not be calculated

Table S6. Steady-state concentrations of •OH, SO4•−, 1O2, and O2•– calculated from solutions that contained sulfamethoxazole and the NB, BA, FFA, and p-BQ probe compounds (all probes present in same solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,NB' (s-1) | 1.22 10-3 | 8.10 10-4 | 7.43 10-4 |
| kobs,BA' (s-1) | 1.25 10-3 | 6.43 10-4 | 5.15 10-4 |
| kobs,FFA' (s-1) | 5.58 10-3 | 1.44 10-3 | 1.06 10-3 |
| kobs,p‐BQ' (s-1) | 5.97 10-4 | 4.83 10-4 | 4.73 10-4 |
| •OHss (M) | 3.13 10-13 | 2.08 10-13 | 1.91 10-13 |
| SO4•–ss (M) | 1.48 10-13 | 6.67 10-14 | 4.84 10-14 |
| 1O2ss (M) | - a | - a | - a |
| O2•–ss (M) | - a | - a | - a |

a: this parameter could not be calculated

Table S7. Steady-state concentrations of 1O2 and O2•– calculated from solutions that contained sulfamethoxazole and the FFA or p-BQ probe compounds (one probe present in each solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,FFA' (s-1) | 2.05 10-3 | 8.29 10-4 | 6.33 10-4 |
| kobs,p‐BQ' (s-1) | 1.40 10-3 | 6.32 10-4 | 4.96 10-4 |
| 1O2ss (M) | 1.71 10-11 | 6.91 10-12 | 5.28 10-12 |
| O2•–ss (M) | 2.77 10-13 | 1.80 10-13 | 1.51 10-13 |

Table S8. Steady-state concentrations of 1O2 and O2•– calculated from solutions that contained sulfamethoxazole and the FFA and p-BQ probe compounds (both probes present in same solution).

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,FFA' (s-1) | 2.10 10-3 | 1.03 10-3 | 6.85 10-4 |
| kobs,p‐BQ' (s-1) | 1.51 10-3 | 7.95 10-4 | 5.86 10-4 |
| 1O2ss (M) | 1.75 10-11 | 8.58 10-12 | 5.70 10-12 |
| O2•–ss (M) | 3.62 10-13 | 2.33 10-13 | 2.13 10-13 |

Table S9. Pseudo-first-order rate constants of the NB, BA, FFA, p-CBA, and p-BQ probe compounds and sulfamethoxazole, steady-state concentrations of •OH, SO4•−, 1O2, O2•–, and Fe(IV), the contribution of each reactive species to sulfamethoxazole degradation, and the second-order rate constant for the reaction between sulfamethoxazole and Fe(IV) measured at variable probe concentrations in the Fe-BC/PS system. These data were recorded for multiple solutions that contained sulfamethoxazole and one probe. Experimental conditions: 0.1 g/L Fe-BC; 2.0 mM persulfate; 200 μM PMSO; 10-30 M NB; 10-30 µM BA; 10-30 µM FFA; 10-30 µM p-CBA; 10-30 µM p-BQ; 50 M sulfamethoxazole; and pH0 3.53.

|  | Probe concentration |  |  |  |
| --- | --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M | Comments |
| kobs,NB' (s-1) | 9.47 10-4 | 8.03 10-4 | 6.49 10-4 |  |
| kobs,SMX' (s-1) | 1.85 10-3 | 1.79 10-3 | 1.58 10-3 |  |
| kobs,BA' (s-1) | 4.80 10-4 | 5.03 10-4 | 7.14 10-4 |  |
| kobs,SMX' (s-1) | 6.63 10-4 | 5.04 10-4 | 4.81 10-4 |  |
| kobs,FFA' (s-1) | 1.52 10-2 | 6.62 10-3 | 1.83 10-3 |  |
| kobs,SMX' (s-1) | 7.11 10-4 | 5.50 10-4 | 4.36 10-4 |  |
| kobs,p‐CBA' (s-1) | 7.89 10-4 | 5.73 10-4 | 8.90 10-4 |  |
| kobs,SMX' (s-1) | 7.60 10-4 | 6.85 10-4 | 6.34 10-4 |  |
| kobs,p‐BQ' (s-1) | 1.87 10-4 | 3.94 10-4 | 5.06 10-4 |  |
| kobs,SMX' (s-1) | 6.73 10-4 | 4.64 10-4 | 3.49 10-4 |  |
| kobs,SMX' (s-1) control | 3.64 10-3 |  |  |  |
| Reactive species concentrations and contributions |  |  |  |  |
| •OHss (M) | 2.42 10-13 | 2.06 10-13 | 1.66 10-14 |  |
| R•OH | 56.5% | 48.1% | 38.8% |  |
| SO4•–ss (M) | 3.21 10-14 | 4.34 10-14 | 8.73 10-14 |  |
| RSO4•– | 14.2% | 19.2% | 38.6% |  |
| 1O2ss (M) | 9.29 10-11 | 2.47 10-11 | 3.72 10-12 |  |
| R1O2 | 0.051% | 0.0136% | 0.00204% |  |
| RFe(IV) | 29.25% | 32.69% | 22.60% |  |
| kFe(IV),SMX″ (M-1 s-1) | 1.07 10-3 | 1.19 10-3 | 2.09 10-3 |  |
| O2•–ss (M) | - a | - a | - a | p-CBA as probe |
| O2•–ss (M) | - a | - a | - a | p-BQ as probe |

a: this parameter could not be calculated

Table S10. Pseudo-first-order rate constants of the NB, BA, FFA, and p-BQ probe compounds and sulfamethoxazole, steady-state concentrations of •OH, SO4•−, 1O2, O2•–, and Fe(IV), the contribution of each reactive species to sulfamethoxazole degradation, and the second-order rate constant for the reaction between sulfamethoxazole and Fe(IV) measured at variable probe concentrations in the Fe-BC/PS system. These data were recorded for one solution that contained sulfamethoxazole and all probes. Experimental conditions: 0.1 g/L Fe-BC; 2.0 mM persulfate; 200 μM PMSO; 10-30 M NB; 10-30 µM BA; 10-30 µM FFA; 10-30 µM p-CBA; 10-30 µM p-BQ; 50 M sulfamethoxazole; and pH0 3.53.

|  | Probe concentration |  |  |
| --- | --- | --- | --- |
| Parameter | 10 M | 30 M | 50 M |
| kobs,NB' (s-1) | 7.57 10-4 | 4.23 10-4 | 3.28 10-4 |
| kobs,BA' (s-1) | 6.13 10-4 | 3.68 10-4 | 3.34 10-4 |
| kobs,FFA' (s-1) | 9.47 10-3 | 2.05 10-3 | 1.79 10-3 |
| kobs,p‐BQ' (s-1) | 3.82 10-4 | 4.75 10-4 | 4.18 10-4 |
| kobs,SMX' (s-1) | 3.12 10-3 | 1.70 10-3 | 1.16 10-3 |
| •OHss (M) | 1.94 10-13 | 1.08 10-13 | 2.53 10-14 |
| R•OH | 52.85% | 54.00% | 18.54% |
| SO4•–ss (M) | 5.31 10-14 | 2.43 10-14 | 2.53 10-14 |
| RSO4•– | 23.49% | 10.75% | 11.19% |
| 1O2ss (M) | 3.57 10-11 | - a | - a |
| R1O2 | 0.0196% | - a | - a |
| O2•–ss (M) | 3.57 10-11 | - a | - a |
| RO2•– | 1.73% | - a | - a |
| RFe(IV) | 0.17% | - a | - a |

a: this parameter could not be calculated

Fig. S1. XRD patterns of the original BC and prepared Fe-BC composites.

Fig. S2. Representative HPLC chromatogram for a solution containing the NB, BA, p-CBA, p-BQ, and FFA probe compounds and sulfamethoxazole.

Fig. S3. UPLC-QTOF-MS spectra for PMS16O18O and PMS18O18O.

Fig. S4. Degradation of PMSO and yield of PMSO2 during Fe-BC/PS treatment. Experiment conditions: [Fe-BC] = 0.05, 0.10, or 0.20 g/L; [PMSO]0 = 200 μM; [PS]0 = 1.0 mM; and pH0 = 3.53.

Fig. S5. Degradation kinetics of (a) NB and (b) BA in single-probe solutions. Experimental conditions: (a) [NB]0 =10, 30, or 50 M; (b) [BA]0 = 10, 30, or 50 M; 0.1 g/L Fe-BC; pH0 = 3.53; and [PS]0 = 1.0 mM.

Fig. S6. Degradation kinetics of NB and BA in a dual-probe solution with initial concentrations of (a) 10 M, (b) 30 M, and (c) 50 M. Other experimental conditions: 0.1 g/L Fe-BC; pH0 = 3.53; and [PS]0 = 1.0 mM.

Fig. S7. Degradation kinetics of FFA, BA, NB, and p-CBA in a multi-probe solution with initial concentrations of (a) 10 M, (b) 30 M, and (c) 50 M. Other experimental conditions: 0.1 g/L Fe-BC; pH0 = 3.53; and [PS]0 = 1.0 mM.

Fig. S8. Degradation kinetics of FFA, BA, NB, and p-BQ in multi-probe solutions with initial concentrations of (a) 10 M, (b) 30 M, and (c) 50 M. Other experimental conditions: 0.1 g/L Fe-BC; pH0 = 3.53; and [PS]0 = 1.0 mM.

Fig. S9. Degradation kinetics of (a) p-BQ and (b) FFA in single-probe solutions with 100 mM MeOH. Experimental conditions: (a) [p-BQ]0 =10, 30, or 50 M; (b) [FFA]0 = 10, 30, or 50 M; [Fe-BC] = 0.1 g/L; pH0 = 3.53; and [PS]0 = 2.0 mM.

Fig. S10. Degradation kinetics of p-BQ and FFA in dual-probe solutions with initial concentrations of (a) 10 M, (b) 30 M, and (c) 50 M and 100 mM MeOH. Other experimental conditions: [Fe-BC] = 0.1 g/L; pH0 = 3.53; and [PS]0 =  2.0 mM.

Fig. S11. The degradation kinetics of (a-c) SMX + FFA, (e-f) SMX + BA, (g-i) SMX + NB, (j-l) SMX + p-CBA, (m-o) SMX + p-BQ in single-probe solutions. Experimental conditions: [Fe-BC] = 0.1 g/L; [PS]0 = 2.0 mM; [SMX]0 = 50 M; [FFA]0 = [BA]0 = [NB]0 = [p-CBA]0 = [p-BQ]0 = 10, 30, or 50 M; and pH0 = 3.53.

Fig. S12. Degradation kinetics of sulfamethoxazole and (a) 10 M, (b) 30 M, and (c) 50 M of the FFA, BA, NB, and p-BQ probe compounds. Other experimental conditions: [Fe-BC] = 0.1 g/L; [PS]0 = 2.0 mM; pH0 = 3.53; and [SMX]0 = 50 M.

Fig. S13. Degradation of PMSO and yield of PMSO2 during Fe-BC/PS treatment at different pH conditions. Experimental conditions: [Fe-BC] = 0.10 g/L; [PMSO]0 = 200 μM; [PS]0 = 1.0 mM; and pH0 = 2.93-6.95.

Fig. S14. Plots of (a) -ln[SMX][SMX]0 and (b) ηlnPMSO0PMSO0-1η[PMSO2] vs. time. Experimental conditions: [Fe-BC] = 0.1 g/L; [PS]0 = 2.0 mM; [PMSO]0 = 10 M; [SMX]0 = 50 M; and pH0 = 3.53.

References

[1] Q.-Y. Wu, Z.-W. Yang, Z.-W. Wang, W.-L. Wang, Oxygen doping of cobalt-single-atom coordination enhances peroxymonosulfate activation and high-valent cobalt–oxo species formation, Proceedings of the National Academy of Sciences, 120 (2023) e2219923120.