The role of Fe(IV) in the zero-valent iron biochar activated persulfate system for treatment of contaminants of emerging concern

Wenwen Gong1, Dandan He2, Xiao Wang2, Yuting Yan2, Dionysios D. Dionysiou3,

Lee Blaney4*, Guilong Peng2,5*

1Institute of Quality Standard and Testing Technology, Beijing Academy of Agriculture and Forestry Science, Beijing 100097, China

2State Key Laboratory of Resource Insects,
College of Sericulture, Textile and Biomass Sciences, Southwest University,

Chongqing, 400715, China

3Environmental Engineering and Science Program, Department of Chemical and Environmental Engineering, University of Cincinnati, Cincinnati, Ohio 45221, USA

4University of Maryland Baltimore County, Department of Chemical, Biochemical, and Environmental Engineering, Baltimore, MD 21250, USA

5Yibin Academy of Southwest University, Yibin, China

*Corresponding authors’ email:

blaney@umbc.edu (L. Blaney);

pengguilong@swu.edu.cn (G. Peng)

Text S1. Analysis of HCHO

HCHO was determined by HPLC with PDA detector after derivatization with DNPH [1]. Briefly, 2.5-mL samples were added to centrifuge tubes containing 100 μL DNPH (250 μM in acetonitrile with 3% H3PO4) and 2.5 mL ultrapure water. After reaction for 30 min at 60 ± 1 ℃ in a water bath, the HCHO concentrations were measured at 365 nm using a mobile phase containing 0.2% acetic acid and acetonitrile (70/30, v/v).

Text S2. Calculation of steady-state concentrations of Fe(IV), SO4•-, •OH, O2•-, and 1O2 in the ZVI-BC/PS system and determination of their relative contributions for contaminant removal

Calculation of steady-state concentrations of Fe(IV), •OH, SO4•-, 1O2, and O2•-

The steady-state concentration of Fe(IV) in the ZVI-BC/PS system was determined using the kinetics of PMSO2 generation from PMSO oxidation. The rate of PMSO2 generation can be expressed as follows:

dPMSO2dt=+kPMSO,FeIV[FeIV]ssPMSO

The yield of PMSO2 is defined as follows:

η=PMSO2PMSOo-PMSO

The PMSO concentration can be expressed as follows:

PMSO=PMSOo-1ηPMSO2

The above equations can be combined and integrated as follows:

dPMSO2PMSO=+kPMSO,Fe(IV)[FeIV]ssdt

dPMSO2PMSOo-1ηPMSO2=+kPMSO,Fe(IV)[FeIV]ssdt=kobsdt

u=PMSOo-1ηPMSO2

-η du=dPMSO2

-η duu==+kPMSO,Fe(IV)[FeIV]ssdt

0t-η duu=0t=+kPMSO,Fe(IV)[FeIV]ssdt

-ηlnPMSOo-1ηPMSO20t==+kPMSO,Fe(IV)[FeIV]sst0t

-ηlnPMSOo-1ηPMSO2PMSOo==+kPMSO,Fe(IV)[FeIV]sst-0

ηlnPMSOoPMSOo-1ηPMSO2==+kPMSO,Fe(IV)[FeIV]sst

ηlnPMSOoPMSOo-1ηPMSO2=kPMSO,Fe(IV)[FeIV]sst=kobst

The steady-state Fe(IV) concentration can be determined as follows:

[Fe(IV)]ss=kobskPMSO,Fe(IV)

In the above expressions, [PMSO] and [PMSO2] are the concentrations of PMSO and PMSO2 at time t, respectively, η is the yield of PMSO2 (i.e., the molar ratio of generated PMSO2 to degraded PMSO), and kPMSO,Fe(IV) is the second-order rate constant for PMSO reaction with Fe(IV) (i.e., 1.23×105 M-1 s-1).

The steady-state concentrations of SO4•- and •OH in the ZVI-BC/PS system were calculated using the NB and BA probe compounds. The degradation of NB and BA in the ZVI-BC/PS process can be expressed as follows:

Integrating the above equations:

Then, [•OH]ss and [SO4•−]ss can be calculated as follows:

In the above expressions, [NB] and [BA] are the concentrations of NB and BA at time t, respectively, kNB,•OH is the second-order rate constant for NB reaction with •OH, and kBA,•OH and kBA,SO4•- are the second-order rate constants for BA reaction with •OH and SO4•-, respectively.

The steady-state concentrations of 1O2 ([1O2]ss) and O2•- ([O2•-]ss) were calculated by competition kinetics in a solution containing 0.05 mM FFA, 0.01 mM p-BQ, and 100 mM MeOH; the MeOH content was included to quench SO4•- and •OH. The [1O2]ss parameter was calculated as follows:

In the above expressions, kFFA,1O2 is the second-order rate constant for FFA reaction with 1O2, and [FFA]0 is the initial FFA concentration (0.05 mM).

With [1O2]ss, the [O2•‐]ss parameter was obtained as follows:

Then, the steady-state concentration of O2•‐ can be calculated as follows:

In the above expressions,  and  are the second-order reaction rate constants for p-BQ reaction with O2•‐ and 1O2, respectively, and [p-BQ]0 is the initial concentration of p-BQ (0.01 mM).

Determination of the contribution of each reactive species

The relative contributions of •OH, SO4•-,1O2, O2•‐, and Fe(IV) (RRS) to the degradation of the target contaminant (TC) can be calculated as follows:

In the above expressions, ,  , and are the second-order rate constants for the target contaminant reaction with •OH, SO4•−, 1O2, and O2•–, respectively.

Fig. S1. (a) Fourier transform infrared spectra and (b) X-ray diffraction patterns of BC and ZVI-BC.

Fig. S2. The observed rate constant for PMSO degradation (kobs) measured for different sample holding times. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S3. HPLC-PDA chromatograms recorded at 215 nm for PMSO and PMSO2 in the presence of different terminators, namely (a) 1/10 mM NaNO2, (b) 1/10 mM NH2OH, (c) 10/100 mM Na2S2O3, and (d) 10/100 mM DMSO. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S4. The PMSO removal efficiency measured in the presence of different reaction terminators, namely (a) 1 mM NaNO2, (b) 1 mM NH2OH, (c) 10 mM Na2S2O3, and (d) 10 mM DMSO, for sample holding times of 0-36 h. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S5. UV-visible absorbance spectra of (a) PMSO and (b) PMSO2.

Fig. S6. Effects of TBA and EtOH on (a) PMSO degradation and (b) PMSO2 production. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S7. The degradation kinetics of PMSO and yield of PMSO2 in the ZVI-BC/PS system in the presence of BA. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; [PMSO]0 = 50 µM; and [BA]0 = 0.1 mM.

Fig. S8. Effects of tiron and FFA on (a) PMSO degradation and (b) PMSO2 production. Experiment conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S9. Degradation (a) profiles and (b) observed rate constants (kobs) for six representative compounds in the ZVI-BC/PS system. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [contaminant]0 = 10 mg L-1.

Fig. S10. Effects of the (a) initial PS concentration and (b) ZVI-BC dose on the yield of PMSO2; changes in the (c) Fe(II) and (d) Fe(III) concentrations during the reaction. Experimental conditions: (a) [ZVI-BC]0 = 50 mg L-1; (b) [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S11. Effect of initial pH on the yield of PMSO2 in solutions with minimal buffer capacity (i.e., no added buffer). Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S12. Effect of pH on (a) PMSO degradation, (b) PMSO2 production, and (c) the yield of PMSO2 in solutions with enough buffer capacity to prevent pH changes during treatment. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; [PMSO]0 = 50 µM; initial sodium acetate (pH 3.5-5.2) =10 mM; and initial sodium borate (pH 7.1) = 10 mM.

Fig. S13. (a) HPLC-PDA chromatograms recorded at 215 nm for DMSO degradation and HCHO formation (after derivatization with DNPH) in the ZVI-BC/PS system, and (b) the measured HCHO-DNPH concentrations for different pH conditions with and without buffer.

Fig. S14. Effects of Cl- and NOM on the yield of PMSO2. Experimental conditions: [ZVI-BC]0 = 50 mg L-1; [PS]0 = 0.5 mM; and [PMSO]0 = 50 µM.

Fig. S15. Effects of different metals on PMSO degradation in solutions (a) without pH control and (b) maintained at pH 7.01. Experimental conditions: [metal]0 = 0.5 mM; [PMSO]0 = 0.1 mM; and [PS]0 = 2.0 mM.

Table S1. Operational parameters for organic contaminant analysis by HPLC-PDA.

| Organic compound | mobile phase |  |  | flow rate (mL/min) |
| --- | --- | --- | --- | --- |
|  | water (0.2% acetic acid) | methanol | detection wavelength (nm) |  |
| BPA | 20 | 80 | 275 | 1.0 |
| SMX | 40 | 60 | 270 | 1.0 |
| p-NBA | 20 | 80 | 270 | 1.0 |
| NB | 40 | 60 | 270 | 1.0 |
| BA | 40 | 60 | 227 | 1.0 |
| p-CBA | 20 | 80 | 234 | 1.0 |
| p-BQ | 20 | 80 | 254 | 1.0 |

Table S2. Second-order rate constants (M-1 s-1) for the reaction of free radical and nonradical reactive species with probe compounds.

| Probe | •OH |  | SO4•‐ | Fe(IV) | O2•– | 1O2 |
| --- | --- | --- | --- | --- | --- | --- |
| Nitrobenzene (NB) | 3.9×109 [2] | - a |  | - a | - a | - a |
| Benzoic acid (BA) | 1.2×109 [2] | 5.9×109 [2] |  | - a | - a | - a |
| PMSO | 3.61×109 [3] | 3.17×108 [3] |  | 1.23×105 [3] | - a | - a |
| FFA | 1.51010 [4] | 1.31010 [4] |  | - a | - a | 1.2×108 [5] |
| p-BQ | 1.2109 [6] | 1.0108 [7] |  | - a | 6.6107 | 9.8×108 [8] |
| BPA | 8.77×109 [9] | 1.37×109 [9] |  | - a | - a | 7.99×106 [10] |

a: not kinetically relevant or unknown

Table S3. Operational parameters for target contaminant and reactive species probe analysis by HPLC-FLD.

| Time (min) | Mobile phase A (water, %) | Mobile phase B (MeOH, %) | Flow rate (mL/min) |
| --- | --- | --- | --- |
| 0.0 | 55 | 45 | 1.0 |
| 5.0 | 55 | 45 | 1.0 |
| 10.0 | 85 | 15 | 1.0 |
| 15.0 | 55 | 45 | 1.0 |

Table S4. The initial and final pH values measured in buffered and unbuffered solutions treated by the ZVI-BC/PS system.

| Reaction | Unbuffered solutions |  |  | Buffered solutions |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 0 min | 3.52 | 5.11 | 7.12 | 7.09 | 5.14 | 3.52 |
| 1 min | 3.42 | 4.52 | 4.35 | 7.09 | 5.14 | 3.52 |
| 2 min | 3.41 | 4.42 | 4.01 | 7.08 | 5.14 | 3.52 |
| 3 min | 3.35 | 4.01 | 3.95 | 7.08 | 5.14 | 3.51 |
| 4 min | 3.34 | 3.65 | 3.88 | 7.09 | 5.14 | 3.52 |
| 5 min | 3.32 | 3.64 | 3.85 | 7.09 | 5.14 | 3.51 |
| 6 min | 3.32 | 3.63 | 3.84 | 7.09 | 5.14 | 3.52 |

References

[1] H. Dong, G. Wei, D. Yin, X. Guan, Mechanistic insight into the generation of reactive oxygen species in sulfite activation with Fe(III) for contaminants degradation, J Hazard Mater, 384 (2020) 121497.

[2] Q.-Y. Wu, Z.-W. Yang, Z.-W. Wang, W.-L. Wang, Oxygen doping of cobalt-single-atom coordination enhances peroxymonosulfate activation and high-valent cobalt–oxo species formation, Proceedings of the National Academy of Sciences, 120 (2023) e2219923120.

[3] H. Dong, Y. Li, S. Wang, W. Liu, G. Zhou, Y. Xie, X. Guan, Both Fe(IV) and Radicals Are Active Oxidants in the Fe(II)/Peroxydisulfate Process, Environmental Science & Technology Letters, 7 (2020) 219-224.

[4] L. Gao, Y. Guo, J. Zhan, G. Yu, Y. Wang, Assessment of the validity of the quenching method for evaluating the role of reactive species in pollutant abatement during the persulfate-based process, Water Research, 221 (2022) 118730.

[5] S. Zhu, C. Jin, X. Duan, S. Wang, S.-H. Ho, Nonradical oxidation in persulfate activation by graphene-like nanosheets (GNS): Differentiating the contributions of singlet oxygen (1O2) and sorption-dependent electron transfer, Chemical Engineering Journal, 393 (2020) 124725.

[6] Z. Liu, S. Pan, F. Xu, Z. Wang, C. Zhao, X. Xu, B. Gao, Q. Li, Revealing the fundamental role of MoO2 in promoting efficient and stable activation of persulfate by iron carbon based catalysts: Efficient Fe2+/Fe3+ cycling to generate reactive species, Water Research, 225 (2022) 119142.

[7] Y. Zhao, M. Song, Q. Cao, P. Sun, Y. Chen, F. Meng, The superoxide radicals’ production via persulfate activated with CuFe2O4@Biochar composites to promote the redox pairs cycling for efficient degradation of o-nitrochlorobenzene in soil, Journal of Hazardous Materials, 400 (2020) 122887.

[8] Z. Liu, S. Pan, F. Xu, Z. Wang, C. Zhao, X. Xu, B. Gao, Q. Li, Revealing the fundamental role of MoO2 in promoting efficient and stable activation of persulfate by iron carbon based catalysts: Efficient Fe2+/Fe3+ cycling to generate reactive species, Water Res, 225 (2022) 119142.

[9] J. Jing, M.N. Pervez, P. Sun, C. Cao, B. Li, V. Naddeo, W. Jin, Y. Zhao, Highly efficient removal of bisphenol A by a novel Co-doped LaFeO3 perovskite/PMS system in salinity water, Science of The Total Environment, 801 (2021) 149490.

[10] Z.-H. Xie, C.-S. He, D.-N. Pei, Y. Dong, S.-R. Yang, Z. Xiong, P. Zhou, Z.-C. Pan, G. Yao, B. Lai, Review of characteristics, generation pathways and detection methods of singlet oxygen generated in advanced oxidation processes (AOPs), Chemical Engineering Journal, 468 (2023) 143778.